## Slide 1
Inovace stávajících nebo tvorba nových metodických a elektronických studijních materiálů v ČJ nebo AJ
Ing. Pavel Holec
Nové možnosti rozvoje vzdělávání na Technické univerzitě v Liberci
Specifický cíl A2: Rozvoj v oblasti distanční výuky, online výuky a blended learning
NPO_TUL_MSMT-16598/2022

## Slide 2: Molar mass distribution

## Slide 3: Molar and relative molecular weight
molar weight
  molar mass
  mass of 1 mole of given molecules [g/mol]
relative molecular weight
  molecular weight
  dimensionless number
    expresses how many times the given molecule is heavier than of the isotope
  somewhat imprecisely it can be viewed as comparing the mass of a molecule to the mass of 1 proton (or 1 neutron)
  Dalton unit
    Da
    in polymer practice usually kDa
    corresponds to the mass of of the isotope because a dimensionless unit is not scientific enough

## Slide 4: Molecular weight of polymers
usually in 103 to 106
Why is it important?
  gives information about the size/length of strings
  size/length of strings
    the higher the weight, the (usually) longer chain
    individual polymers can only be compared after conversion (according to measured weights)
      e.g. the yellow trimer is heavier but shorter than the green heptamer
      the molecular weight is thus directly related to the degree of polymerization P
this is not unambiguous information (badly includes branching or cyclic structures)
  however, usually the higher the number, the larger (longer) the string
50
150
350
450
700
relative weight

## Slide 5: A few definitions
macromolecules of synthetic polymers usually do not have the same size (molar mass)
  are so-called non-uniform (polydisperse)
  are a mixture of polymer homologues
    macromolecules with the same chemical composition but different molar masses
  weight distribution more or less continuous
some polymers (usually natural substances, e.g. proteins) can be made up of precisely sized macromolecules
  a polymer of macromolecules of uniform molar mass is called uniform (mondisperse)

## Slide 6: Why do we care about molar mass?
fundamentally affects the physical, physico-chemical and chemical properties of materials
  the nature of the material
    oligomers tend to be liquid
    short polymers tend to be waxy and non-solid
    extremely long tend to be stiffer to rigid
  dissolution rate
  viscosity of the solution or melt
  elasticity
  reactivity
    the shorter the chains, the greater the relative number of end groups
When stirring, boiled penne is easier to handle than boiled spaghetti due to the difference in their length.

## Slide 7: Average molar mass of polymers
molar mass of non-uniform polymers (each macromolecule generally has a different one)
  it is solved by appropriate averaging
there are several types of averages
  numerous
  viscosity
  mass
  z
    supposedly centrifugal - from the German centrifuge
    then z+1 (expansion of the z-mean)
each kind of diameter gives emphasis to differently sized molecules
  e.g. z-averages mainly consider the longest fibers

## Slide 8: Table of average molar masses
name |  | symbol | expression |  | 
number… | average molar mass |  |  |  | 
viscosity… |  |  |  |  | 
mass… |  |  |  |  | 
z… (centrifugal) |  |  |  |  | 
z + 1… |  |  |  |  | 
name |  | symbol | expression |  | 
number… | average molar mass |  |  |  | 
viscosity… |  |  |  |  | 
mass… |  |  |  |  | 
z… (centrifugal) |  |  |  |  | 
z + 1… |  |  |  |  | 
xi … molar fraction; wi … mass fraction; a … Mark-Houwink constant

## Slide 9: Visualization of molar mass distributions
basically two options
  differential curve
    shows how many molecules have a given molar mass
  integral (cumulative) curve
    shows how many molecules have a given molar mass and smaller
M
frequency
M
relative frequency
100 %

## Slide 10: Differential distribution curve of molar masses
shows how many macromolecules have a given molar mass
usually some variant of the log-normal distribution
  however, it can also be other (e.g. double-peaked, etc.)
M
frequency

## Slide 11: Differential distribution curve of molar masses
the numerically averaged mass curve is shown
then other diameters on it
it is always true that
Mn
Mv
Mw
Mz
Mz+1
M
frequency

## Slide 12: Distribuční křivky molárních hmotností

## Slide 13: Dispersity index
formerly called polydispersity
corresponds to the proportion of mass centers of mol. hmm compared to numerically medium
  since the numerator (Mw) is always greater than or equal to the denominator (Mn), the non-uniformity index is always greater than 1
gives information about how non-uniform the system is
  if it is close to 1, then the molecules are similar in length
    Đ around 1.1 to 1.3 are still considered practically uniform
  if 50 is needed, we have a decently non-uniform system

## Slide 14
M
frequency
D = 30
M
frequency
M
frequency
D = 1
M
frequency
D = 1,5
frequency
D = 5
M

## Slide 15: An example of calculating molecular weights
Let us have 7 moles of uniform polybutylene terephthalate (PBTF) with a molar mass of 654 g/mol, 3 moles of PBTF with a molecular weight of 210 g/mol and 9 moles of PBTG with a mass of 87 g/mol. Calculate the number average, weight average, z and z+1 average molar mass of a given PBTF as well as the non-uniformity index. Discuss the result.
polymer homolog | amount of substance (mol) | molecular weight
A | 7 | 6540
B | 3 | 2100
C | 9 | 870

## Slide 16: Example 2
polymer homolog | amount of substance (mol) | molecular weight
A | 1 | 4000
B | 1 | 100000

## Slide 17: Example 3
polymer homolog | amount of substance (mol) | molecular weight (kDa)
A | 5 | 4
B | 2 | 100

## Slide 18: Example 4
polymer homolog | amount of substance (mol) | molecular weight (kDa)
A | 5 | 4
B | 1 | 120

## Slide 19: Example 5
polymer homolog | amount of substance (mol) | molecular weight (kDa)
A | 250 | 4
B | 1 | 1000

## Slide 20: Example 6
polymer homolog | amount of substance (mol) | molecular weight (kDa)
A | 171 | 4
B | 71 | 12
C | 37 | 24
D | 23 | 46
E | 11 | 112

## Slide 21: Fractionation of polymer homologues
isolation of polymer homologues from a mixture
  individual polymer homologs can almost never be isolated
    remember the definitions of a polymer (removing a few units won't affect their properties - So how could I isolate them if I can't find any property in which they differ physically or chemically?)
  rather, polymer molecules with a very narrow distribution (e.g. Đ = 1.1) are obtained

## Slide 22: Fractionation methods
precipitation
  the longer the chain, the more easily it is precipitated by the addition of the wrong solvent
  I dilute the initially perfect polymer solution with a non-solvent and gradually remove the precipitated polymer
dissolution
  the opposite of the precipitating technique
gel permeation chromatography (GPC)
  the polymer solution flows through a column (tube) in which there is a gel with defined pores and the whole thing is carried by a suitable liquid (the so-called mobile phase in which the polymer is soluble)
  small macromolecules flow into the pores during this and stay behind the large ones that do not fit into the pores
  the smaller the molecule, the slower it flows
  at the end of the column, I gradually remove the polymer solution with a narrower distribution

## Slide 23: Determination of molar mass
can be divided by
  output values
  absolute
    by measuring I get the molar mass value
  relative
    I need a standard to determine the exact value
output (which average value you get)
  Mn
    end group method
    osmometry
    ebuloscopy
    cryoscopy
    mass spectroscopy
  Mv
    rheometry
  Ms
    light scattering
    sedimentation
practically always only for soluble polymers

## Slide 24: Methods measuring Mn
end group method
  absolute method of determination
  each (unbranched) macromolecule has two ends (often reactive) → if I find the number of end groups, I get the exact number of macromolecules
  I can, for example, use a dye (preferably green, because I like it the most), which binds only to the ends, and then spectrophotometrically determine how much of it binds
osmometry
  membrane or in the vapor phase
  osmotic pressure depends on the size of macromolecules
  we let the solvent penetrate into the polymer solution through the semi-permeable membrane and after equalizing the osmotic and hydrostatic pressures we determine the molar mass

## Slide 25: Methods measuring Mn
ebuloscopy
  a small addition of a nonvolatile solute to a solvent will lower its boiling point
  this change in boiling point is proportional to the change in molar concentration
cryoscopy
  a small addition of a non-volatile solute to a solvent will lower its melting point
  this change in melting point is proportional to the change in molar concentration
mass spectrometry
  absolute method
  chop a macromolecule into pieces (by ionization)
  I filter ions (e.g. through a quadrupole) according to the ratio of their charge and mass (z/m)
  I will measure the frequency of ions with a given z/m ratio
  I will find out the spectrum and from it the molar mass of the original macromolecule

## Slide 26: Methods measuring Mv
viscometry
  relative method
  viscosity dependent on concentration and molar mass
    imagine that you are mixing 500 g of said penneis and 500 g of unbroken long spaghetti in a 5 l pot of hot water - one will surely be much harder to stirr
  multiple measurement methods
  capillary
    e.g. Ubbehlohde viscometer (A)
  ball
    the object descends through the solution and I measure the speed of descent
    e.g. Höppler viscometer (B)
  rotational
    rotational viscometers or rheometers (C)
flow index
  for melts
  how many (grams) of polymer melt will flow through a defined nozzle at a defined temperature and pressure
  does not indicate the molar mass, but the flow properties of the polymer depending on the molar mass
B
A
C

## Slide 27: Methods measuring Mw
light scattering
  absolute
  scattering of light on small particles (molecules)
  very sensitive to dirt (dust, scratches on optical elements, etc.)
  the wavelength of the radiation used must be
  the intensity of the scattered radiation depending on the viewing angle, the concentration of the solution and the mass average molar mass
    depending on the size of the macromolecular balls, different kinds of scattering occur

## Slide 28: Thank you for your attention