## Slide 1
Inovace stávajících nebo tvorba nových metodických a elektronických studijních materiálů v ČJ nebo AJ
Ing. Pavel Holec
Nové možnosti rozvoje vzdělávání na Technické univerzitě v Liberci
Specifický cíl A2: Rozvoj v oblasti distanční výuky, online výuky a blended learning
NPO_TUL_MSMT-16598/2022

## Slide 2: Synthesis of polymers

## Slide 3: Three conditions of monomer polymerizability
in order for a monomer to polymerize, it must meet three conditions:
chemical
  a structure capable of forming chains
thermodynamic
  an appropriate reaction is taking place
kinetic
  the polyreaction must be faster than the other reactions
  system can be activated

## Slide 4: 1. Chemical condition
monomers must be at least difunctional (f at least 2)
  at least two groups capable of binding to other molecules
multiple bond
suitable functional groups
cycle with a heteroatom
f=2
f=3

## Slide 5: 2. Thermodynamic condition
the Gibbs energy must decrease during the reaction
  assumption of spontaneous reaction (lower energy of the resulting system)
∆𝐺 < 0
ΔG … change in Gibbs (free) energy
∆𝐺 = ∆𝐻 − 𝑇∆S
  ΔH … enthalpy change
  T … thermodynamic temperature
  ΔS … entropy change

## Slide 6: 2. Thermodynamic condition
ΔH … enthalpy change
  transferred energy (heat) at constant pressure
    exothermic reaction (ΔH < 0) – energy leaves the system
    endothermic reaction (ΔH > 0) – energy enriches the system
  fundamentally influenced by the structure of the monomer
  usually energy is released (exothermic reaction)
ΔS … entropy change
  degree of system disorder (the larger, the more disordered)
  usually ΔS < 0
    monomers arrange themselves into chains
    the exception is the tearing of large cycles, where ΔS is slightly higher than 0
Pieter Bruegl – The Fight Between Carnival and Lent (1559)

## Slide 8: 2. Thermodynamic condition
∆𝐺 = 0 = ∆𝐻 − 𝑇∆S
ΔH | < 0 | < 0 | > 0 | > 0
ΔS | < 0 | > 0 | < 0 | > 0
 | Tc | always | never | Tf
Tc … ceiling temperature
  after exceeding it, polymerization stops, because ΔG>0
Tf … floor temperature
  the reaction does not run until it is exceeded, since ΔG>0
ceiling vault in Kladruby (Santiny)
paving in the rotunda of St. Wenceslas in Prague (MatFyz)

## Slide 9: 3. Kinetic condition
the polyreaction must be faster than other reactions (e.g. termination of growth, depolymerization, etc.)
  monomers must preferentially grow into macromolecules and not something else
  vgrowth ≫ vrest
the monomer must be activatable
  a reactive intermediate must be formed
    dependent on the monomer structure
  activation
    radicals
    ions
    complexes

## Slide 10
Polymer synthesis
chain-growth
step-growth
radical
ionic
anionic
cationic
coordination (polyinsertion)
ring opening
Ziegler-Natta
metallocene
polycondensation
polyaddition

## Slide 11: Chain and step reactions
chain-growth
  polymerization takes place only at the growth center (*)
  monomers react at a limited number of sites (dark green)
step-growth
  monomers can react with monomers, oligomers and polymers
2
3
4
1
1
1
1*
1
2*
1
1
1
3
1
3*
1
4
4
1
4*
2
5
1
1
1
1
1
2
3
3
3
5
5
5
5

## Slide 12: Chain-growth polyreaction
repeated attachment of monomer molecules to growth centers (radicals, ions, complexes)
three groups of reactions are usually repeated (it is not always a single reaction, but rather a series of reactions): initiation, propagation, termination
chain reaction mechanisms (mostly named after the growth center)
  radical, ionic, coordination (polyinsertion), ring opening
2
3
4
1
1
1
1*
1
2*
1
1
1
3
1
3*
1
4
4
1
4*

## Slide 13: The chain reaction mechanism is influenced by:
chemical structure of monomers
  multiple bonds
    usually double, but triples can also be found
  bond polarization
  size of substituents
    bulky substituents may sterically hinder the reaction
  stress in circles (if I have cyclic monomers)
mechanism of initiation and or catalysis
  monomer dependent
ability to stabilize reaction intermediates
  dependent on the monomer and reaction mechanism

## Slide 14: Dependence of polymerization chain reaction degree on conversion
polymerization degree P
  = number of monomeric units in the macromolecule
monomer conversion
  = proportion of reacted monomer units
  100% conversion therefore means complete reaction of the reaction mixture
chain polyreactions
  capital P even with a small conversion
  it no longer increases much at higher conversions
conversion [%]

## Slide 15: Characteristic features of chain polyreaction
molecules grow by repeated addition to the active site
the monomer concentration decreases gradually during the polymerization
  the concentration of growing molecules is small (10-8 to 10-3 mol)
long reaction times are not necessary for the formation of a high molecular weight polymer
  the time required to form a long macromolecule is on the order of a few seconds

## Slide 16: Chain-growth polyreactions - radical
one of the most widespread synthetic polyreactions
LDPE, PS, PMMA, SR, PVAc
the general course of a radical reaction
initiation
promotion
termination
  "The concept of free radicals was unknown in 1920. Well, maybe in politics, but not in chemistry.” Herman Francis Mark

## Slide 17: Initiation (radical polyreactions)
initiation = formation of a growth center
usually homolytic cleavage of the initiator bond to form radicals
  radical = a molecule with an unpaired electron
    is marked with a dot (lone electron)
    generally extremely reactive (unstable)
cage effect
  after homolytic cleavage, it can happen that the resulting radicals located close to each other react together and the radicals thus disappear
such reactions do not lead to the formation of initiator molecules
with reactive monomers, the polyreaction sometimes takes place spontaneously
they must therefore be stabilized (so that they do not react already in the storage container)
dibenzoylperoxide
ABIN

## Slide 18: 1. Initiation
the radical's electron is highly reactive
  electrons always want to be in pairs (remember gas molecules, e.g. H2)
it wants to make an electron pair with any other electron
it also pulls it out of an already existing electron pair
  the more weakly bound such an electron is, the easier it will be
    eg π electrons of a double bond
initiator cleavage Ini-Ini → Ini· + ·Ini
the creation of a growth center Ini· + H2C=CH2 → Inic-CH2-CH2·

## Slide 19: Ways of initiation
thermal
radiation
  photoinitiation (visible radiation)
  high-energy (X-ray, α, β, γ, n0)
oxidation-reduction
electrochemical
non-initiating reaction (influence of the cage effect)

## Slide 20: 2. Propagation
represents the growth of the (macro)molecule itself
the growth center is still transferred to the end of the chain
Ini-CH2-CH2· + H2C=CH2 → Ini-CH2-CH2-CH2-CH2·
Ini-CH2-CH2-CH2-CH2· + H2C=CH2 → …

## Slide 21: 3. Termination
the disappearance of the growth center (given molecule)
  two radicals form an electron pair (the radical disappears)
  radical jumps to another molecule (radical does not disappear)
recombination (pairing)
  a single bond is formed between the radicals
[CH2]n· + ·[CH2]m → [CH2]n+m
disproportion
  one molecule will provide a hydrogen and the other an electron to the radical
[CH2]n· + ·CH2-CH2[CH2]m → [CH2]n + CH2=CH2-[CH2]m
  „I‘ll be back.“

## Slide 22: Mechanism of disproportionation

## Slide 23: Transfer reactions
there is no disappearance of the reaction center
the reaction center is transferred to a new location on the macromolecule or to a new macromolecule
  intramolecular
  intermolecular
always accompanied by hydrogen transfer
creation of branched structures
  e.g. LDPE
initiator (not iodine)

## Slide 24: LDPE
low density (low density) PE
highly branched structure
  How is it possible that the difunctional monomer ethylene is able to form a branched structure?
    transfer reactions
produced under high pressures by radical polymerization
chemically resistant, mechanically weak

## Slide 25: Chain-growth polyreactions - ionic

## Slide 26: Chain-growth polyreactions - ionic
varies with the type of growing active center
  cationic (polyisobutylene)
  anionic (formaldehyde)
comparison with radical polymerization
  more selective
  sensitive to the presence of impurities (e.g. water)
  more expensive (more complicated)
  chain growth cannot be terminated by recombination or disproportionation (equally charged active centers repel each other)

## Slide 27: Kinetic condition for vinyl monomers
the substituent stabilizes the reactive intermediate (macroion)
  thus determines the mechanism of the polyreaction
a combination of inductive and mesomeric effects
  inductive effect
    electron displacement along the σ bond
    caused by the different electronegativities of the atoms
  mesomeric effect
    electron displacement along the π bond
    caused by the conjugation of the π electrons of the substituent and the vinyl double bond
    usually stronger than inductive effect
PVA
PVAc
PS
PVC

## Slide 28: Inductive and mesomeric effect
the resulting shift of electrons from or to the substituent (Sub) given by a combination of inductive and mesomeric effects
the mesomeric effect is usually stronger than the inductive one
  the exception is for the –X halides, which have such a strong inductive and such a weak mesomeric that they generally behave more according to the inductive
due to the I and M substituent on vinyl, electrons are pushed to the double bond or, conversely, pulled away from the double bond
  this will subsequently affect whether the double bond will be partially positively charged (has less electron density) or partially negatively charged (higher electron density)
  depending on whether it will react cationically or anionically

## Slide 29: Inductive effect (I)
given by the different electronegativity of neighboring atoms
positive (+I)
  alkyl, alkenyl, phenyl, ether, amine
negative (-I)
  halogen, carbonyl, nitro
δ+
δ-
δ+
δ-
δδ-
δδ+
Y→C→C→C
X←C←C←C
Electron acceptoric substituents (I-)
Electron donating substituents (I+)

## Slide 30: Mezomeric effect (M)
electron displacement along the π bond
  M+ pushes electrons to, M- on the contrary, away
  caused by the conjugation of the π electrons of the substituent and the vinyl double bond
  conjugation
    stabilization caused by overlapping of neighboring π electrons or a lone electron pair
  identification in the molecule
    double bonds or double bond and free elec. a pair of atoms next to each other
usually stronger than inductive
  except for the halides, which are more inductive because π e- are much more mobile than σ e-

## Slide 31: Mezomeric effect (M)
positive (+M)
  increasing electron density
  it can be recognized by the fact that a less electronegative atom is attached to a more electronegative atom (e.g. ←O←C- or ←S ←C-))
negative (-M)
  decreasing electron density
  it can be recognized that a more electronegative atom is bound to a less electronegative atom (e.g. →C→O- or →C→S-)
Electron acceptoric substituents (M-)
Electron donating substituents (M+)
R = alkyl or H
R = alkyl or H

## Slide 32: Examples of action of I and M
styrene
  phenyl certainly has I+ and M+, so the whole will push electrons towards the vinyl double bond
  however, the benzene nucleus is capable of stabilizing many things, so it can behave in several ways
vinyl chloride –Cl
  chloride has a strong I- and a weak M+, so the whole will withdraw electrons from the double bond towards the chloride (except when M is weaker than I)
nitrile –CN
  nitrile induces both I- and M-, so the unit must withdraw electrons from the double bond
methyl ether –O–CH3
  the oxygen of the methyl ether will provide I-, but the methyl ether has M+, so the whole will push the electrons towards the double bond (M is stronger than I here)

## Slide 33: Cationic polymerization
the growth center has a positive charge (carbocation)
the Y substituent pushes electrons to the vinyl double bond
  the latter is therefore more electron-rich and can attack with an electron-acceptor initiation particle
little used in industry
  too much reactivity
  macroion instability
  solvent costs
examples
  polyisobutylene
  poly(1,1-dimethylethylene)
termination usually by a transfer reaction
initiation
propagation
tertiary carbocation
secondary carbocation
primary carbocation
increase in carbocation stability

## Slide 34: Anionic polymerization
the growth center has a negative charge (carbon anion)
the X substituent withdraws electrons from the vinyl double bond
  the double bond is thus electron-poor and more easily attackable by an electron-donating particle
used more in industry
  costs of solvents and initiators
examples of reacting monomers
  styrene, butadiene, isoprene, vinyl ester, methacrylate, cyanoacrylate, cyclic monomers
  a typical example is instant glue (cyanoacrylates)
usually ending in a transfer reaction
initiation
propagation
tertiary carbanion
secondary carbanion
primary carbanion
increasing the stability of the carbanion

## Slide 35: Chain-growth polyreactions - coordination

## Slide 36: Chain-growth polyreactions - coordination
otherwise also polyinsertion
  production of tactical polymers
  other methods are usually short on this
Ziegler-Natt catalysts
  a transition metal salt (eg TiCl4) and an organometallic compound of element III. main groups (e.g. Al(CH2CH3)3)
  isotactic polymers
metallocene catalysts
  sandwich molecules (metal cation is enclosed between aromatic anions)
  isotactic or syndiotactic polymers

## Slide 37: Ziegler-Natta catalyst

## Slide 38: Tacticity of macromolecules
the arrangement of stereoisomeric centers in the main chains of macromolecules
  stereoisomerism - occurs in asymmetric molecules with carbon having different substituents on all four bonds
fundamentally affects crystallinity
  and thus also mechanical properties, temperature behavior, etc.
syndiotactic
atactic
isotactic

## Slide 39: 1. Constitution (regularity)
regular macromolecule
  obtained by regular repetition of the constitutional unit
  head-to-heel arrangement only
only regular polymers can (but don't have to) be semicrystalline
head-to-tail
head-to-head (or tail-to-tail)

## Slide 40: HDPE, UHMWPE
linear macromolecules
high crystallinity and therefore also density
extraordinary mechanical properties
HDPE – 200,000 to 500,000 g/mol
  high density (high density) PE
UHMWPE – 6,000,000 g/mol
  Ultra high molecular weight PE
  chains contain over 200,000 mers
HDPE
UHMWPE

## Slide 41: Polypropylene (PP)
exclusively isotactic
  atactic is practically not used because it is an unusable waxy substance
fibers, pipes, packaging material, disposable products
semicrystalline

## Slide 42: Chain-growth polyreactions – Ring opening

## Slide 43: Chain-growth polyreactions - Ring opening
denoted by the abbreviation ROP
  in principle, it is not a reaction mechanism itself, but a group of different reactions (radical or ionic) that have in common that they start from cyclic monomers
thermodynamics plays a big role
  usually the most important thing is the tension in the circle (the larger the circle, the less stable the circle and the more likely we will be able to activate it)
  the least stable rings are 3 and 4 membered, then around 9
  the presence of a heteroatom or a multiple bond is required
  with large circles almost without steric stran
    the entropy change ΔS also starts to play a role in them
      it can be even higher than 0, because the opening of the ring increases the mobility of the new ends and so the entropy increases

## Slide 44: Chain-growth polyreactions - Ring opening
can be polymerized radically (unsaturated heterocycles) or ionically
cyclic monomers
  lactones
  lactams
  heterocycles with sulfur or silicon
Chart: Steric strain in cycloalkanes
| 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16
 | 115.1 | 110.1 | 26 | 0.5 | 26.2 | 40.5 | 52.7 | 51.8 | 47.3 | 17.2 | 21.5 | 8 | 7.8 | 8

## Slide 45: Reaction of caprolactone and caprolactam
caprolactone (cyclic ester)
caprolactam (cyklic amide)
polycaprolactone (PCL)
polyamide 6 (PA 6)

## Slide 46: Step-growth polyreactions

## Slide 47: Step-growth polyreactions
mutual reaction of functional groups of monomers, oligomers and polymers in an "all with all" way
the reaction mixture contains chains of various lengths, from monomer to finished macromolecules
can be divided into
  polycondensation
  polyadiction
2
5
1
1
1
1
1
2
3
3
3
5
5
5
5

## Slide 48: Dependence of degree of polymerization of stepwise polyreactions on conversion
polymerization degree P
  = number of monomeric units in the macromolecule
monomer conversion
  = proportion of reacted monomer units
  100% conversion therefore means complete reaction of the reaction mixture
stepwise polyreactions
  slow growth of the polymerization degree
  higher degree of polymerization only at high conversions
conversion (%)

## Slide 49: Step-growth polyreactions
a low molecular weight product is always formed
  low molecular weight product (d) is usually water, hydrogen halide, methanol or ammonia
often equilibrium reactions (must affect equilibrium)
  it means that the yield of such reactions tends to be low
homopolymerization
  hydroxycarboxylic acids (PES), aminocarboxylic acids (PA)
heteropolymerization
  e.g. dicarboxylic acid with diol (PES) or diamine (PA)

## Slide 50: Carothers equation (for linear polymerization)
let's have a bifunctional monomer A-B (where A reacts only with B)
  the number of monomer molecules before the reaction starts is Nbeginning
    during the polyreaction, N decreases
    monomers react to become oligomers or polymers
  the number of unreacted monomer molecules is Nunreacted
  the degree of conversion p corresponds to the proportion of reacted monomer molecules to their original number
  (numerically) the average degree of polymerization Pn corresponds to :
  from this follows the so-called Carothers equation of the dependence of the degree of polymerization on the degree of conversion of the monomer:
Consequence of the Carothers equation If we want to prepare macromolecules of high molar mass, we have to drive the reaction to extreme degrees of conversion
conversion (%)
P

## Slide 51: Dependence of the molecular size distribution on the degree of conversion p (Flory distribution curves)
P
relative frequency
relative frequency
P

## Slide 52: Equilibrium constant I
  usually, equilibrium reactions
    equilibrium given for the const. temperature by the equilibrium constant K
      in common esterifications they are from 0.1 to 10
    unbalanced above 10000, balanced up to 100
e.g.
a small equilibrium constant means that the degree of monomer conversion will be low
  → a low degree of conversion means that the degree of polymerization will be low
  → a low degree of polymerization means that the useful properties of the polymer will be poor
    it is necessary to break the equilibrium of the reaction (usually by removing a low-molecular-weight product)

## Slide 53: Equilibrium constant II
if amino acid molecules react (forming water and amide -CONH-) with each other, the following applies to their functional groups (-NH2 for amino, -COOH for carboxylic):
  where (among other things) the concentration of amine groups must match the concentration of carboxyl groups, so that:
  the concentration of the resulting amide groups -CONH- is equal to the degree of conversion p of the original reacting groups:
  at the same time, the concentration of reacting groups corresponds to the amount of unreacted groups (i.e. 1-p):
K
p

## Slide 54: Equilibrium constant III
  after adjustment:
  the number average molar mass Pn is:
  Then:
  at high conversion (p approaches 1) we can write:

## Slide 55: Equilibrium constant IV
a consequence of the problem of low equilibrium constants
  enabling the formation of macromolecules always with a low degree of polymerization even at (theoretically) 100% conversion p
solution:
  removal of low molecular weight product (concentration reduction)

## Slide 56
Example of a theoretical reaction of
5-aminopentanoic acid chloride with itself (homopolycondensation)

## Slide 57
terephthalic acid
ethane-1,2-diol
Example of the reaction of terephthalic acid with ethane-1,2-diol (heteropolycondensation)

## Slide 58
terephthalic acid
ethane-1,2-diamine
Example of the reaction of terephthalic acid with ethane-1,2-diamine (heteropolycondensation)

## Slide 59: Polycondensates - PET
can be derived from terephthalic acid or its chloride
  terephtaoyl chloride is used more often because the low molecular weight HCl product is more easily distilled off

## Slide 60: Polycondensates - epoxy resins
reaction of bisphenols and epichlorhydrin (known locally as epic)
modeling, grinding and grinding, dental medicine

## Slide 61: Polycondensates - phenoplasts
synthetic resins based on phenol and aldehydes
phenol (trifunctional - 2× ortho, 1× para) + formaldehyde (bifunctional)
depending on the phenol:formaldehyde ratio, temperature and pH, the following are formed:
  alkaline pH + excess formaldehyde → resol → resit (after cross-linking)
  acidic pH + excess phenol → novolac
the most famous is Bakelite

## Slide 62: Resol
mixture of oligomers with reactive methylol groups (-CH2OH)
  molar mass around 500 to 2000 g/mol (from 2 to about 10 mers)
the hydroxyl group of the phenol directs the substitution on the aromatic nucleus to the ortho and para positions
  base-catalyzed reaction of phenol with formaldehyde
    molar ratio less than 1 (usually 0.8 - 0.9)
    mono-, di- and trimethylolphenols are formed
liquid or solid substances (according to structure)
may be water soluble (generally not)

## Slide 63: Examples of condensations of methylolphenols
retained methylol group (they can react further)

## Slide 64: Resins
resins are formed by cross-linking resols
  takes place in an acidic environment at higher temperatures (180 °C)
    methylene (-CH2-) or methyl ether bridges (-CH2-O-CH2-)
    the higher the temperature, the more methylene bridges prevail over methyl ether bridges
brown-red coloration caused by the formation of quinone methides (their conjugated double bonds absorb visible radiation) during the thermal splitting of water from methylolphenols during cross-linking

## Slide 65: Novolac
oligomers resulting from the acid-catalyzed reaction of formaldehyde with phenol, with an excess of phenol
  formaldehyde:phenol ratio = 0.75 to 0.85:1
  molar mass up to approximately 1000 g/mol (again units to lower tens of mers)
do not contain methylol groups
  there is an excess of phenol, so the formaldehyde will react all of it
  thanks to their absence, they are more stable
they are thermoplastic substances
their cross-linking produces phenol-formaldehyde resins

## Slide 66: Polycondensates - phenol-formaldehyde resins
cross-linking of novolacs with formaldehyde-releasing substances (e.g. hexamethylenetetramine with water) at higher temperatures (160 °C)
  methylene bridges
  benzylamine bridges (Ph-CH2-NH-)

## Slide 67: Polycondensates - aminoplasts
again, one reactant is formaldehyde (as in phenoplasts)
  the second is a nitrogenous compound:
    urea (up to tetrafunctional)
    melamine (up to six functions)
nebo
formaldehyde
urea
melamine

## Slide 68: Reaction of formaldehyde with urea or melamine
depending on the reaction conditions:
  mono- to tetramethylolurea
  mono- to hexamethylolmelamine
mono-
di-
tri-
tetra-
tri-
hexa-

## Slide 69: Cross-linking of aminoplasts
again increased temperature and acidic environment
again methylene and methyl ether bridges
due to the high functionality of urea and melamine, a very dense network is created

## Slide 70: Polycondensates - polysulphide rubber
reaction of alkyl dihalides with inorganic polysulfides
oil-resistant rubbers, the torment of students during laboratory work
y

## Slide 71
Table of reaction groups and their polycondensation products |  | 
-OH | -COOH | polyester
-OH | -COOR | 
-OH | -COOX | 
 | -X | polyether
 | -OH | 
-NH2 (may also apply to secondary) | -COOH | polyamide
 | -COOR | 
 | -COOX | 
-SiOH | -SiOH | polysiloxane
-CHO | aromatic alcohol | phenol-formaldehyde resins
 | urea derivates | urea-formaldehyde resins

## Slide 72: Step-growth polyreactions - polyaddition
reaction without the formation of by-products
  without changing the total composition of the product (only a change in structural units)
    in a sense the simplest reaction to invent
    I will evaluate the type of new bond and describe the rest so that there is nothing left
the balance of such reactions is usually strongly shifted in favor of the products
ring-opening polymerization (ROP) is sometimes also classified here
  however, they show signs of chain polymerization

## Slide 73: PUR
insulation, adhesives, mounting foams, artificial leather
many possible side reactions:
  foam PUR
    isocyanate + water
  cross-linked PUR
    isocyanate + amine
diisocyanate
diol (generally polyol)
polyurethane
rigid part
soft part

## Slide 74: Industrial methods of polymerization

## Slide 75
not only the reaction mechanism affects the polymerization outcome
during polyreactions, heat is usually generated (sometimes so high that the whole thing can catch fire or explode)
  given that the conversion of most monomers to polymer has a negative enthalpy change ΔH and the temperature increases during the reaction
generally four methods of polymerization:
Industrial methods of polymerization
Industrial methods of polymerization
bulk (in the monomer phase)
solution
suspension
emulsion

## Slide 76
takes place directly in the monomer phase
  I add an initiator to the monomer and let it react
  radical or ionic
if the resulting polymer is soluble in its monomer, I get an increasingly viscous solution, which eventually solidifies (a real block of polymer - hence the older name of the method)
if the emerging polymer is not soluble in its monomer, a fine powder precipitated in the monomer is formed (I get a powder, so the label block polymerization is not entirely appropriate)
high product purity
  there is nothing else except the initiator
difficult cooling
  the reaction usually produces a lot of heat and I may not be able to cool it down inside the growing polymer
  thermal decomposition of the resulting polymer or boiling of the monomer may occur (possibly catching fire)
1. Bulk polymerization
monomer
initiator
initiator
initiator

## Slide 77
in order to dissipate the reaction heat and cool the whole, I dissolve the monomer in a suitable cooling liquid and add the initiator
  the monomer must therefore be soluble in the liquid
  radical, ionic or coordination polymerization
easy cooling
  lower product purity
  there is a lot of solvent
lower average molar mass
  lots of solvent molecules reduce the chance of the growth center hitting another monomer
  growth centers are transferred to solvent molecules
if the polymer is soluble in the cooling liquid, I get a viscous solution
  adhesives and coatings
  or I can pour a non-solvent into the mixture and precipitate the polymer (precipitation reaction)
if the polymer is insoluble in the cooling liquid, it precipitates and I get a fine powder
2. Solution polymerization
cooling liquid
initiator
initiator
initiator
monomer
monomer
monomer
monomer
monomer
monomer
monomer

## Slide 78
called pearl or bead polymerization
at the beginning we have an emulsion of the monomer phase (monomer + initiator dissolved in it) in the immiscible phase of the cooling liquid
  monomer phase mostly non-polar, cooling liquid polar (e.g. water)
the polyreaction creates a suspension of solid spherical polymer particles in a cooling liquid (therefore suspension or bead)
I stabilize the emulsion by stirring
as with the soup with oil meshes, by stirring I make sure that the meshes stay small and do not combine into larger ones
  if the droplets made a big drop, I wouldn't cool it
  the droplet size is usually around 1 mm
  the amount and size of the droplets depends mainly on the mixing speed
3. Suspension polymerization
monomer + initiator
monomer + initiator
monomer + initiator
cooling liquid

## Slide 79
the amount of coolant makes it easy to cool down
I have to add stabilizers
  during the growth of the macromolecules the droplets become sticky and would stick together, so I cover them on the surface with something to prevent them from sticking together
    either a substance clinging to the surface of the droplets (like flouring dough on a roll)
    or something to increase the viscosity of the coolant so that the droplets cannot get close to each other
  it reduces the purity of the product
used e.g. for PS, PVC, PMMA
3. Suspension polymerization

## Slide 80
monomer
monomer
monomer
cooling liquid
based on a monomer immiscible with the cooling liquid, in which the initiator and emulsifier (= surfactant, surfactant) are dissolved
  above the critical micellar concentration, the emulsifier forms micelles in which the monomer is enclosed (it doesn't want to be in the cooling liquid and likes to stuff itself inside the micelles)
  compared to suspension micelles, the micelles are mainly stabilized by the emulsifier and not so much by mixing or additives
the polyreaction takes place inside the micelles, where the monomer is practically pure
micelle size is in units of μm (compared to 1 mm for suspension)
the polyreaction starts when the initiator gets into the droplet
4. Emulsion polymerization
initiator
initiator
initiator
initiator
surfactant
surfactant
surfactant

## Slide 81
higher average molar masses
easy cooling
after all, a less pure product
the result of the polyreaction is the so-called latex
  = stable emulsion of polymer particles with a size of about 1 μm dispersed in a cooling liquid (hence emulsion polymerization)
  suitable for paint materials
  a polymer can be obtained by precipitation
usually for latex/rubber
4. Emulsion polymerization

## Slide 82
  Emulsion polymerization reactor (here for PVDF aqueous emulsion) A – Reactor, B – Stirrer, C – Stream splitter, D – Monomer dispenser, E – Stirrer motor with stirring resistance control, F – Safety sensors and fuses, G – Bottom valve

## Slide 83: Thank you for your attention