## Slide 1
Inovace stávajících nebo tvorba nových metodických a elektronických studijních materiálů v ČJ nebo AJ
Ing. Pavel Holec
Nové možnosti rozvoje vzdělávání na Technické univerzitě v Liberci
Specifický cíl A2: Rozvoj v oblasti distanční výuky, online výuky a blended learning
NPO_TUL_MSMT-16598/2022

## Slide 2: Copolymers

## Slide 3: Copolymer
otherwise also a heteropolymer
  the opposite is a homopolymer
macromolecular substance formed from at least two different types of monomers (usually 2 or 3 types)
  individual monomers are called comonomers
according to the number of comonomers, we distinguish bipolymerization (2), terpolymerization (3), etc.
enantiomers are generally not considered different monomers
common in natural polymers (heteropolysaccharides, proteins, lignin, etc.)
they also have considerable technical significance
  acrylonitrile-butadiene-styrene rubber (ABS)
  butadiene styrene rubber (BSR)
  copolymers of ethylene with vinyl acetate (EVA)

## Slide 4: Pseudocopolymers
there are polymers classified as homopolymers, although there are more different monomer units in their structure, which can be given by:
  by different course of monomer reactions (e.g. 1,2 and 1,4 reactions of butadiene)
  or an imperfect conversion (e.g. residues of acetate groups in PVA)
enantiomers are not considered different monomers
  e.g. the reaction of the reaction of the enantiomeric mixture of R-methyloxirane and S-methyloxirane leading to atactic polymethyloxirane is not taken as copolymerization

## Slide 5: Importance of copolymers
modification of the properties of the final product
  solubility
  tenacity
  hardness
  abrasion resistance
  elasticity
  optical properties
  thermal stability
  option to add networkable groups
  improving the dispersibility of additives (pigments, etc.)

## Slide 6: Types of polymers according to measurements
structure |  | term |  | abbreviation
 | … | homopolymer | … | polyA
- | … | general copolymer | … | poly(A-co-B)
 | … | random (statistical) | … | poly(A-stat-B)
 | … | alternating | … | poly(A-alt-B)
 | … | block | … | poly(A-block-B)
 | … | grafted | … | poly(A-graft-B)
A
A
A
A
A
A
A
A
B
A
A
A
B
B
A
B
B
A
B
A
B
A
B
A
A
A
A
A
B
B
B
B
A
A
A
A
A
A
A
A
B
B
B
B
B
B
B
B
B
B
B
B

## Slide 7: Polymerization leading to copolymer
copolymer |  | polyreaction
random (statistical) | … | radical
alternating | … | radical, polycondensation
block | … | ionic
grafted | … | radical, ionic

## Slide 8: Copolymerization reaction
polymerization of at least two different types of monomers
e.g.:
  poly(ethylene-co-propylene)
  poly(styrene-co-butadiene)
  poly(vinylidene chloride-co-vinyl chloride)
  poly[imino(1,6-dioxohexane-1,6-diyl)iminohexane-1,6-diyl] (PA6,6)

## Slide 9: Radical bipolymerization
three types of reactions (same as for radicals)
  initiation
  promotion
  termination
in general, the rules of radical homopolymerization apply, but complicated by the possibility of a larger amount of reaction

## Slide 10: Initiation of radical bipolymerization
homolytic decay of initiator I produces 2 radicals R·
however, two growth centers may arise
  one on the M1 monomer and the other on the M2 monomer

## Slide 11: Promotion of radical bipolymerization
thus, bipolymerization may appear to be not much more complicated than homopolymerization
  however, the multiplication of possible reactions occurs again in the case of promotion
if only the last unit of the growth chain affects the addition of a new measure, 4 reactions can occur
  rate constants correspond to individual reactions kij

## Slide 12: Termination of radical bipolymerization
this time the same as for homopolymerization
  recombination (pairing)
    a single bond is formed between the radicals
  [CH2]n· + ·[CH2]m → [CH2]n+m
  disproportion
    one molecule will provide a hydrogen and the other an electron to the radical
  [CH2]n· + ·CH2-CH2[CH2]m → [CH2]n + CH2=CH2-[CH2]m

## Slide 13: The ratio of incorporated mers in the copolymer
it is determined by the amount of incorporated mers or, conversely, the rate of decrease of the given monomers
it's supposed, that
  monomers are consumed only for the growth reaction (initiation is thus neglected)
  the concentration of radicals is unchanged
    if a new one arises, another must disappear (and vice versa)
    it is referred to as the stationary state condition of bipolymerization
    applies as follows:
    the equation can be understood, for example, as the rate of disappearance of radicals -Mi· is the same as the rate of their formation

## Slide 14: Constant concentration of radicals
monomer is consumed only in growth reactions (theoretically)
growth reaction | radical balance of growth centers
 | radical –M1· of the growth center does not disappear, because it is replaced by another –M1
 | radical –M1· of the growth center disappears, but a new radical is formed –M2·
 | radical –M2· of the growth center disappears, but a new radical is formed –M1·
 | radical –M2· of the growth center does not disappear because another one replaces it –M2·
growth reaction | radical balance of growth centers
 | radical –M1· of the growth center does not disappear, because it is replaced by another –M1
 | radical –M1· of the growth center disappears, but a new radical is formed –M2·
 | radical –M2· of the growth center disappears, but a new radical is formed –M1·
 | radical –M2· of the growth center does not disappear because another one replaces it –M2·
When one perishes, the other must arise, and when the other perishes, the first arises again.

## Slide 15: Radical ratio of growth centers
the rate of incorporation of individual mers must somehow correspond to the representation of individual radicals -M1· and –M2·
can be simply derived from the steady state condition

## Slide 16: The ratio of incorporated mers in the copolymer (Part II)
it is determined by the amount of incorporated mers or, conversely, the rate of decrease of the given monomers
the rate of decrease (concentration) of a given comonomer corresponds to the rate of all reactions that consume it (in a given time):

## Slide 17: The ratio of incorporated mers in the copolymer (Part III)
share of rates of change in comonomer concentrations:
copolymerization parameters
  express the ratio of the rate of homopolymerization of comonomer i to the rate of copolymerization i and y
homopolyameration
copolyameration

## Slide 18: Copolymerization equation
by adjusting the equation of the proportions of the rates of change of the comonomer concentrations using the copolymerization parameters ri, the so-called copolymerization equation is created
the resulting composition of the copolymer thus depends on:
  proportional representation of comonomers M1 and M2 in the reaction mixture
  copolymerization parameters r1 and r2
applies in general, but since the ratio of comonomers usually changes over time, it is usually not possible to calculate the resulting polymer composition from it only according to the ratio of comonomers in the reaction batch

## Slide 19: The ratio of incorporated mers in the copolymer (Part IV)
the reactivity of the growth centers can depend not only on the last measure, but also on the penultimate one
  the so-called penultimate effect
the whole process is then complicated by the necessity of using new copolymerization parameters ri‘
+
+
+
+

## Slide 20: The ratio of incorporated mers in the copolymer (Part V)
the significance of the values of the copolymerization parameters ri
  > 1 … M1 binds preferentially to the growth center ending in –M1·
  ≈ 1 … M1 binds to a growth center ending in –M1· about as fast as it binds to a growth center ending in –M2·
  < 1 … M1 binds preferentially to the growth center ending in –M2·

## Slide 21: Copolymerization diagrams
the product of the copolymerization parameters r1r2 is more often used to estimate the composition of the copolymer
  it is expressed by so-called copolymerization diagrams
axes of diagrams
  mole fraction of the composition of the reaction mixture fi
    number of comonomer molecules M1 and M2
  by the molar fraction of mers incorporated into the growing Fi chains
    number of built-in measures m1 and m2

## Slide 22: Homopolymerization or block copolymerization
when both r1 and r2 are significantly higher than 1
  it means that mainly homopolymerizations occur
in radical polymerization, two homopolymers are formed (this is not copolymerization)
block copolymers may occur in the case of ionic ones

## Slide 23: Alternating copolymerization
occurs in two (three) cases:
  fň) homopolymerization growth does not take place (comonomer M1 does not react with growth center –M1· and M2 does not react with center –M2·)
  bž) M1 incapable of homopolymeric growth (the comonomer M1 does not react with the growth center –M1·)
  dř) the same case as bž) – it is only a reversed labeling of comonomers
fň) | bž) | dř)
fň) | bž) | dř)

## Slide 24: Alternating copolymerization
r1 = r2 = 0
  perfectly (strictly) alternating
  comonomers are always able to react only with the other comonomer and not with themselves
  if one of the comonomers in the reaction mixture runs out, the reaction stops
r1 = 0; r2 = 0,1
  mostly alternating
  comonomers react predominantly with the second comonomer
  it ceases to be perfectly alternating when the composition of the reaction mixture is deviated (e.g. it will only consist of comonomers)
F1
the homopolyreaction here takes place 10 times worse than the heteropolyreaction

## Slide 25: Side topic: Heteropolyamides
the case of strictly alternating copolymers
  polycondensation reaction (not yet resolved radical)
comonomers can (due to their chemical nature) only react with the opposite (not with each other)
PA 46, PA 66, PA 69, PA 610, PA 612, PA1012
they are copolymers because they are formed from two comonomers
  some consider them homopolymers because these comonomers cannot be made into the corresponding homopolymers, but the general definition classifies them as copolymers
homopolyamide
heteropolyamide

## Slide 26: Statistical (ideal) copolymerization
occurs when the preceding applies and at the same time:
  lň) comonomer M1 prefers homopolyreaction and M2 prefers heteropolyreaction
  tž) (similar to that) comonomer M1 prefers heteropolyreaction and M2 prefers homopolyreaction
  hř) homopolyreaction and heteropolyreaction take place at the same speed for both comonomers
lň) | tž) | hř)
lň) | tž) | hř)

## Slide 27: Statistical (ideal) copolymerization
r1 = 5; r2 = 0,2
  ideal non-azeotropic copolymerization
r1 = 0,2; r2 = 5
  ideal non-azeotropic copolymerization
r1 = r2 = 1
  ideal azeotropic copolymerization
  the composition of the copolymer is dependent only on the composition of the reaction mixture
  not very common

## Slide 28: Non-ideal copolymerization
occurs when the preceding applies and at the same time:
the most common case of copolymerizations
bň) | hž) | fř)
bň) | hž) | fř)

## Slide 29: Non-ideal copolymerization
r1 = 0,52; r2 = 0,12
  non-ideal azeotropic copolymerization
r1 = 0,04; r2 = 0,01
  non-deal azeotropic copolymerization
r1 = 55; r2 = 0,01
  non-ideal non-azeotropic copolymerization

## Slide 30: Azeotropic and non-azeotropic copolymerization
azeotrope
  the composition of the copolymer is identical to the composition of the handle (fce y = x)
azeotropic copolymerization
  its curve intersects the imaginary line segment of the ideal azeotropic copolymerization (at a point other than the starting or ending point)
nonazeotropic copolymerization
  its curve does not intersect the imaginary line segment of the ideal azeotropic copolymerization (at a point other than the starting or ending point)
azeotropic points

## Slide 31: Block copolymerization (ionic)
ionic copolymerization the most common
  a homopolymer with live ends (capable of further reaction – living polymerization) of the chains is produced
  after all the monomer is consumed, another suitable monomer is added and the reaction is continued
  I can repeat with the same or new comonomers until I get bored
l
l
polymeration
l
l
polymeration
1.
2.
l
l

## Slide 32: Block copolymerization – from prepolymers
another possibility is the use of prepolymers
  they are oligomers with end groups capable of further reactions
  after they are mixed, a reaction occurs and a polymer is formed
this is how e.g. poly(ester-block-urethane) is prepared
  it is based on macrodiol and macrodiisocyanate
    in the illustration below, A can be, for example, an –OH group and B can be an –NCO group
A
A
B
B
A
A
A
A
B
B
B
B
polymeration
B
A

## Slide 33: Block copolymerization – joining of chains
another possibility is the linking of individual suitable prepolymers with bifunctional low molecular weight substances
  these low molecular weight substances are called chain linkers
A
A
B
B
A
A
A
A
B
B
B
B
polymeration
B
A
C
C
C
C
C
C
C
C
C
C

## Slide 34: Block copolymerization - mastication
mechanochemical syntheses can also be used
  mechanically (for example on unevenly rotating calenders or by ultrasound) the chains of two or more homopolymers (all together) are broken, radicals are formed at the ends of the fragments and these cause their relinking
    this is referred to as mastication
  they are radicals, so not only recombination, but also other reactions take place
  from two torn homopolymers, both homopolymers and a block copolymer are generally formed back
mech. stress
recombination
homopolymer
homopolymer
kopolymer

## Slide 35: Grafting
usually radical, sometimes ionic
radicals
  uses transfer reactions (remember branching in LDPE)
  I dissolve the finished polymer with monomer (M) and initiator (I)
  initiate monomer polymerization (heat, UV, photoinitiation)
  with a sufficient concentration of radicals, transfer reactions and thus grafting begin to occur
the products of such reactions are mixtures of both homopolymers and a graft copolymer
  extra pure products are usually not needed (sometimes units of % grafted molecules in the polymer are sufficient)
M
M
M
M
M
M
Ini
initiation
transfer reactions
Ini
M

## Slide 36: A simplified scheme of graft polymer synthesis
A-A-A-A-A-A-A-A-A
A-A-A-A-A-A-A-A-A
A-A-A-A-A-A-A-A-A
A-A-A-A-A-A-A-A-A-A
A-A-A-A-A-A-A-A-A-A-A-A-A
dissolving polymer A
adding monomer B and initiator I*
B
B
B
B
B
B
B
B
B
B
B
I*
I*
I*
A-A-A-A-A-A-A-A-A
A-A-A-A-A-A-A-A-A
A-A-A-A-A-A-A-A-A
B-B-B-B-
B-B-B-B-
B-B-B-B-
B-B-B-B-
B-B-B-B-
B-B-B-B-B-B
B-B-B-B-B-B
B-B-B-B-B-B
B-B-B-B-B-B

## Slide 37: Grafting of oxirane chains on PA
increase in wettability and sorption properties
  significant in the modification of about 15% of the amide groups

## Slide 38: Copolymers in practice
NBR
  acrylonitrile butadiene (nitrile) rubber
  non-oily in non-polar solvents (fuel hoses)
SBS
  styrene-butadiene-styrene (tough PS)
  block polymer (anionic polymerization)
  usually styrene:butadiene = 3:7
  styrene provides hardness, butadiene flexibility and toughness
  partially cross-linked

## Slide 39: Copolymers in practice
ABS
  acrylonitrile-butadiene-styrene
  amorphous thermoplastic material (e.g. for the production of LEGO bricks)
VC+VAc
  vinyl chloride + vinyl acetate
  VAc content reduces Tm (over 25% it is already hot melt adhesives)
SAN
  styrene-acrylonitrile
  styrene provides hardness, acrylonitrile chemical resistance and flexibility

## Slide 40: Thank you for your attention