## Slide 1
Inovace stávajících nebo tvorba nových metodických a elektronických studijních materiálů v ČJ nebo AJ
Ing. Pavel Holec
Nové možnosti rozvoje vzdělávání na Technické univerzitě v Liberci
Specifický cíl A2: Rozvoj v oblasti distanční výuky, online výuky a blended learning
NPO_TUL_MSMT-16598/2022

## Slide 2: Chemical reactions of polymers

## Slide 3: Chemical reactions of polymers
divided according to the effect on the length of macromolecule chains
  polymerization degree without change = polymer analog reactions
  halogenation, esterification, hydrolysis or alcoholysis of substituents, intramolecular cross-linking...
  can be further divided into reactions:
    changing the original substituents
    introducing new substituents
change in degree of polymerization
  increasing
    graft
    block copolymerization
    networking
  reducing
    degradation (heat, mechanical stress, oxidative, photochemical, hydrolytic, enzymatic)
    depolymerization
73 10 111 2 2

## Slide 4: I. Polymer analogue transformations
take place in polymers with a stable main chain
  preferably pure carbon
take place in solution or swollen polymer
  easier contact of reacting substances
better performed in a nitrogen atmosphere
  preventing oxidative cleavage of the backbone of macromolecules

## Slide 5: Preparation of PVA from PVAc
cannot be prepared from PVA
  enol form shifts to keto form (here to aldehyde)
it is prepared from polyvinyl acetate by alcoholysis
  the amount of replaced groups describes the so-called degree of hydrolysis
    usually between 80% and 99.9%
    from a certain degree of hydrolysis, further increases impair water solubility
methanol

## Slide 6: Preparation of polyvinyl acetals
PVF (polyvinyl formal)
PVB (Polyvinyl Butyral)
  it is used as glue, foil (e.g. for gluing layers of safety glass) and varnishes
condensation of PVA in acidic medium or hydrolysis with aldehyde in acidic medium
- H2O
in fact, the departing water is not formed by the labeled atoms, but it is enough to give an idea

## Slide 7: Polyvinyl acetal
as with PVA and polyvinyl acetals, there is not always a complete conversion of the original substituents
  of PVA there remain VAc and VA groups
  the number of residual groups is therefore given
PVB
vinyl acetate
vinyl alcohol
vinyl acetal
PVB
PVA

## Slide 8: PVB

## Slide 9: Preparation of cyclized PAN
high chain stability (heat resistance)
conjugated double bonds (possibly conductivity) in a ladder-like arrangement
is formed by intramolecular cross-linking of PAN
it is one of the starting materials for the preparation of pure carbon fibers
PAN

## Slide 10: Introduction of new substituents
halogenation, halogensulfonation, hydrogenation, nitration, sulfonation

## Slide 11: Chlorosulfonated PE
CSM or less commonly CSPE
  the meaning of the M at the end means saturated hydrocarbon chain (but still quite misterious symbol)
production of synthetic rubber from PE
  introduction of Cl2 and SO2 into a boiling solution of LDPE in tetrachloromethane with initiator (ABIN)
  chlorine content approximately 25-40%
  crosslinked with sulfur or peroxides (non-crosslinked is also used)
does not proceed very well in the crystalline phase (hence LDPE)
  inhomogeneous product in the case of more crystalline PE

## Slide 12: Modification of PA
introduction of formaldehyde
  increase in humidity

## Slide 13: Cellulose reaction
cellulose
  the most represented (by mass) polymer in the world
  part of plant bodies (together with hemicelluloses and lignin)
  a homopolysaccharide of β-D-glucopyranoses linked by a β-1,4 glycosidic (glycosidic) bond

## Slide 14: Viscose fibers and foils
Abbreviation CV
also referred to as regenerated cellulose
preparation
  pulverized cellulose is converted to natron cellulose (sodium salt of cellulose) under the influence of NaOH solution
  by carbon disulfide (CS2) it is converted to cellulose xanthogenate
  it is an esterification with xanthogenic acid and thiolthiocarbonic acid
  dissolution of xanthogenate in NaOH (formation of viscous solution → viscosity)
  ripening (about a week)
  filtration
  regeneration in a H2SO4, ZnSO4 and Na2SO4 bath
  extrusion through nozzles (fibers - viscose silk) or foil casting (cellophane)
xanthogenic acid
thiolthiocarbonic acid

## Slide 15: The formation of regenerated cellulose
NaOH
NaOH
CS2
H2SO4
ZnSO4 Na2SO4
cellulose
sodium cellulose
cellulose xanthogenate
viscose (xanthogenate dissolved in NaOH solution)
regenerated cellulose (viscose silk or cellophane)
not necessarily all OH groups must react (the primary will almost certainly, the secondary may not)

## Slide 16: Cellulose esters
cellulose acetate (CA)
  introduction of acetate groups to cellulose hydroxyls
    hardly usable when all three hydroxyls react → necessity of additional hydrolysis back to –OH
    average number of acetates per glucopyranose unit between 2.2 – 2.9 (out of 3 total)
introduction of additional ester groups
  propionate (CP)
  mixed esters acetopropionate (CAP), acetobutyrate (CAB)

## Slide 17: Cellulose nitrate
it is another cellulose ester
is formed by the action of HNO3 on cellulose in the presence of another acid (most often sulfuric, less phosphoric or acetic)
  with theoretical esterification of all 3 OH groups, the N content would be about 14.14%
    is not produced
  nitrates with N content 10 – 11%
    paint materials, celluloid (after addition of camphor)
  nitrates with an N content of 11.8 – 12.5% with resins and solvents
    nitro lacquers
  nitrates with N content 12 – 13.5%
    explosives (smokeless gunpowder)
incorrectly nitrocellulose (difference between nitro and nitrate)

## Slide 18: Cellulose esters
term | abbreviation | general structure | R substituents
cellulose | - |  | -H
cellulose acetate | CA |  | 
cellulose propionate | CP |  | 
cellulose acetopropionate | CAP |  | a
cellulose acetobutyrate | CAB |  | a
cellulose nitrate | CN |  | 

## Slide 19: Cellulose ethers
for the production of adhesives and thickeners
  some soluble in water
dependent on the degree of substitution
examples
  (methyl)cellulose
  (ethyl)cellulose
  (hydroxyethyl)cellulose
  (carboxymethyl)cellulose

## Slide 20: Cellulose ethers
term | abbreviation | general structure | R substituents
cellulose | - |  | -H
(methyl)cellulose | MC |  | 
(ethyl)cellulose | EC |  | 
(ethylhydroxy)cellulose | HEC |  | 
(karboxymethyl)cellulose | CMC |  | 

## Slide 21: Mercerization of cellulose
formation of sodium salt due to NaOH (not all OH groups need to react)
  takes place under voltage
  (does not apply to viscose)
  the kidney-shaped cross-section of the fiber changes to a round one
  improvement:
    tensile strength
    shine
    digestibility
    the quality of the sauce
NaOH

## Slide 22: II. Reactions accompanied by a change in the degree of polymerization

## Slide 23: Reactions accompanied by a change in the degree of polymerization
grow
  graft
  linking macromolecules (block polymers)
  for both see the previous lecture Copolymers
networking
  connecting polymer chains using covalent bonds to form a spatial network
  loss of solubility and fusibility
    they do not dissolve in the solvent, they can at most swell (swell)
  lose thermoplasticity (become infusible)
  resistance to elevated temperatures, chemicals, hardness increases
    the more densely cross-linked, the worse the penetration of molecules of low molecular weight substances into the structure
  swelling and humidity decrease
  used in:
    rubbers
    polyolefins
    PES resins
    epoxy resins
    phenol formaldehyde resins
    superabsorbent polymers

## Slide 24: Crosslinking of polyolefins
crosslinking with peroxides (at a temperature of 200 °C in a nitrogen atmosphere)
  radical reaction
  fission or chain branching can also occur (radicals are very reactive)
the degree of crosslinking can be improved by introducing suitable comonomers during polymer production
  depending on the desired network density, I can build a few multifunctional groups into the macromolecules, which I will later use for crosslinking the whole

## Slide 25: Crosslinking of polyolefins
crosslinking with peroxides (at a temperature of 200 °C in a nitrogen atmosphere)
  radical reaction
  chain breaking or branching can also occur (radicals are very reactive)
2
2

## Slide 26: Radiation cross-linking
radical cross-linking again
high-energy radiation ruptures molecules to form radicals, which then cross-link macromolecules with each other
  possible problem with the penetration of radiation into the depth of the product

## Slide 27: Crosslinking of unsaturated PES resins
solutions of linear unsaturated PES in monomers polymerizing by chain mechanism
  are prepared by polycondensation of mixtures of saturated and unsaturated dicarboxylic acids (or their derivatives) with diols
    maleic, fumaric or phthalic acid (or their anhydrides)
      ensure the unsaturation of the resulting product
    ethane-1,2-diol or propane-1,2-diol
  monomers are most often styrene, less often methyl methacrylate, vinyltoluene, etc.
the radical reaction of unsaturated PES resins with styrene creates styrene bridges (crosslinking)

## Slide 28: Crosslinking of unsaturated PES resins
maleic, fumaric or phthalic acid (or their anhydrides)

## Slide 29: Crosslinking of unsaturated PES resins
initiator (radical)

## Slide 30: Crosslinking of phenol-formaldehyde polymers - resins
resins are formed by cross-linking resols
  takes place in an acidic environment at higher temperatures (180 °C)
    methylene (-CH2-) or methyl ether bridges (-CH2-O-CH2-)
    the higher the temperature, the more methylene bridges prevail over methyl ether bridges
brown-red coloration caused by the formation of quinone methides (their conjugated double bonds absorb visible radiation) during the thermal splitting of water from methylolphenols during cross-linking

## Slide 31: Cross-linking of phenol-formaldehyde polymers – phenol-formaldehyde resins
cross-linking of novolacs with formaldehyde-releasing substances (e.g. hexamethylenetetramine with water) at higher temperatures (160 °C)
  methylene bridges
  benzylamine bridges (Ph-CH2-NH-)

## Slide 32: Cross-linking of aminoplasts
again increased temperature and acidic environment
again methylene and methyl ether bridges
due to the high functionality of urea and melamine, a very dense network is created

## Slide 33: Sulfur crosslinking of elastomers - vulcanization
the most common cross-linking reaction
  action of sulfur and heat (around 140 °C)
can be used for practically all butadiene homopolymers and copolymers
the product of elastomer vulcanization is rubber
  other additives are added to the final products (fillers, dyes, UV stabilizers, etc.)
resulting properties dependent on the amount of sulfur
  is determined in parts by weight of sulfur per hundred wt. rubber parts (phr)
    soft rubber - up to about 4 phr
    semi-hard – usually 12 to 25 phr
    hard (ebonite) – 25 to 50 phr

## Slide 34: Sulfur crosslinking of elastomers - vulcanization
it doesn't work very well without other substances
in this case, the sulfide bridges are quite long after vulcanization (40 to 50 sulfur atoms)
  bridges on neighboring atoms and cyclic sulfide structures do not particularly help physically
  therefore accelerators and activators are used
the average number of sulfur atoms is reduced to about 1.6
  no cyclic structures or bridges are formed on neighboring atoms
activators
  ZnO, stearic acid
  accelerators
  2-mercaptobenzthiazole, tetraalkylthiuram disulfide, zinc salts of dialkyldithiocarbamates

## Slide 35: Sulfur crosslinking of elastomers - vulcanization
probably takes place through an ionic mechanism
  observe the positive charge to understand the reaction
  the interesting thing is that both double elastomers do not participate in the cross-linking reaction, but only one - the other thus remains in the structure

## Slide 36: Ionomers
crosslinking bonds are not covalent but ionic (or hydrogen)
copolymer of ethene and 5-10% acrylic or methacrylic acid
  carboxyl groups can be neutralized to form an acrylate or methacrylate salt (Na, Ca, Mg, Zn, Al, Ba)
  it is not a static network and monovalent ions (Na) contribute to its strength
with enough temperature I can disrupt the network without degrading the macromolecules themselves
  can be melted and after cooling I get the network again
physically they behave similarly to thermoplastic elastomers

## Slide 37: Depolymerization and degradation of polymers

## Slide 38: Depolymerization of polymers
the opposite of polymerization reactions
  there is a gradual splitting off of the mers from the ends of the macromolecules
  molecular weight decreases gradually
sometimes the monomer can be recovered in this way
  Opus Magnum of ecologically based macromolecular chemists
  the Czech product ERVOeco comes a little closer to that
depolymerization is usually caused by higher temperature
  it must not be overdone, otherwise the polymer would begin to degrade
  sometimes it can also be started chemically (e.g. depolymerization of cellulose due to alkaline pH)
they dopolymerize well with polymers that
  have quaternary carbon (e.g. PMMA),
  or can stabilize a reactive intermediate with a conjugated structure (e.g. PS)

## Slide 39: Polymer degradation
primary bonds are split at a random location in the chain
  occurs when the energy of the external action is greater than the strength of the bonds in the main chain
accompanied by a deterioration of the useful properties of the polymer
  in particular, there is a reduction in strength, a change in color, the polymer becomes more brittle,...
occurs by:
  heat
  radiation (light, UV, high energy)
  oxygen
  water
  enzymes
  mechanical stress
  most often a combination of the previous one

## Slide 40: The principle of depolymerization and degradation
M
M
M
M
M
M
M
M
M
M
E
M
M
M
M
M
M
M
M
M
M
E
M
M
M
M
M
M
M
M
M
M
M
M
M
M
M
M
M
M
M
E
E
M
M
M
M
M
M
M
M
M
M
M
M
M
M
M
M
M
M
depolymeration
degradation

## Slide 41: Thermal degradation in an inert atmosphere
effective heat
  generally pyrolysis
first the chains are split
subsequently sufficiently low molecular weight substances escape in the form of gases
  stable low molecular weight substances can form liquid oily products
  eventually the residue will char (if it has a carbon base)
  can occur together with depolymerization (PS)
sometimes the bonds of the substituents to the main chain are weaker than those in the main chain
  primary cleavage of substituents then occurs
T

## Slide 42: Thermooxidative degradation
combination of heat and oxygen
  if the temperature is high enough, it will usually burn at some stage
initiation
  depends on structural defects
  the presence of benzene nuclei or double bonds (they like to absorb radiation)
  the accelerating element of initiation are transition metal compounds
    Fe, Mn, Ni, Cu
bond breakage
  most often tertiary carbons are attacked by oxygen compounds
  hydroperoxides are formed, which break down the chains

## Slide 43: Photooxidative degradation
it is not necessary for the polymer to burn, even energy from the sun will suffice (even if it will go slower)
  occurs when the radiation energy overcomes the strength of the bond
  the rate of decay depends on the wavelength of the light and the energy of the radiation
    less than 330 nm (i.e. UV) is required for cleavage of C–C or C–H bonds
    in the case of double bonds, a light wavelength of 350 nm is sufficient
    therefore, UV absorbers are added to polymers
the rate of photochemical reactions depends on the presence of groups that absorb in the 300-350 nm region
  aldehydes, ketones, hydroperoxides
radiation is absorbed by groups of atoms, subsequently radicals are formed and the chain breaks down

## Slide 44: Hydrolysis and alcoholysis
these are reactions in which the main medium is water (or alcohol) and ions
  thus, an –OH group is usually formed at the point of bond breaking
  can be considered the opposite of some condensation reactions (e.g. esterification or amidification)
polymers with heteroatoms in the chains are most often subject to hydrolysis
  cellulose, PES, PA, PUR
use in the processing of PET waste
  splitting into starting substances
application in healthcare
  absorbable surgical sutures
    polyglycolic acid
    polycaprolactone

## Slide 45: Mechanical demolition
it is mainly used during the so-called plasticization (mastification)
  facilitates processing
  reduces and unifies molecular weights
degradation occurs through mechanical action
  while extruding the polymer from the nozzle at its sharp mouth
  by kneading between two rollers rotating at unequal speeds
usual for rubber compounds

## Slide 46: Polymer stabilization
reducing the rate and impacts of degradation
two methods
  absorptive
    the stabilizer absorbs the energy or influence of the harmful effect
      in the process they can be consumed (retarders) or can be regenerated
        they will use the incoming energy for their own transformation, and the rest of the unused energy is no longer sufficient to degrade the polymer bonds
        the second option is to stabilize the intermediate so well that it does not want to react further (stabilization of radicals by aromatics)
    carbon black, UV absorbers, antioxidants etc.
  reflexive
    the stabilizer prevents harmful influences from coming into contact with the polymer
coatings, foils, films
UV

## Slide 47: Thank you for your attention