## Slide 1
Inovace stávajících nebo tvorba nových metodických a elektronických studijních materiálů v ČJ nebo AJ
Ing. Pavel Holec
Nové možnosti rozvoje vzdělávání na Technické univerzitě v Liberci
Specifický cíl A2: Rozvoj v oblasti distanční výuky, online výuky a blended learning
NPO_TUL_MSMT-16598/2022

## Slide 2: Elastomers

## Slide 3: Elastomers
definition:
  a material which, within its application temperature, is capable of quickly, mostly reversibly deforming with a small force by at least 100% of its original length
    its elastic limit is low at a high rate of relative deformation
  exhibits rubbery properties usually over a wide range of temperatures
can generally be divided into:
  rubber
    elasticity ensured mainly by chemical knots
  thermoplastic elastomers
    elasticity ensured mainly by physical knots
    ionomers are a special kind

## Slide 4: Rubbery elasticity
entropy driven plot
  between the nodes of the network (chemical or physical), the chains are coiled into the most energetically stable (poorest) form of the so-called statistical coils
  due to the mechanical force, the coil untangles and the chains are stretched - but this is not an energetically advantageous arrangement of the chains
  after the end of the stress, the chains want to return to the energetically advantageous arrangement of the coils and thus tangle back to approximately their original form
    the coils will certainly not be rolled in the same way, but their size (radius of gyration) will be the same as in the initial state
F
statistical coil
F
from the point of view of entropy too ordered (so disadvantageous)

## Slide 5: Knots
a place in the structure of a macromolecule that firmly fixes two or more chains or parts thereof together
  chemical knot
    it can be a chemical bond or a binding side chain
    the nature of cross-linking reactions
  physical
    really knotted strings
    crystallites
they support elastic behavior

## Slide 6: Graph of deformation
dependence of stress on the elongation of the body
  by tension we mean the force F on the cross-section of the body S
    therefore it has a unit of pressure
  first reversible (elastic) deformation
  perfectly flexible to A
  almost perfectly flexible to B
    then irreversible (plastic) deformation
  finally rupture (F)
Hooke's law
  direct relationship between stress and strain
  valid until A, usable until B
    elastomers have a proportionality constant E (Young's modulus of elasticity) in the order of units to low tens
A | … | limit of proportionality
B | … | elastic limit
C | … | upper yield limit
A
C
D
E
F
B
stress σ (MPa)
relative deformation ε
D | … | lower yield point
E | … | strength limit
F | … | breaking point
Hooke's law

## Slide 7: Tensile test result
A | … | limit of proportionality
B | … | elastic limit
C | … | upper yield limit
A
C
D
E
F
B
stress σ (MPa)
relative deformation ε
D | … | lower yield point
E | … | strength limit
F | … | breaking point
Hooke's law

## Slide 8: Shapes of tensile curves
stress σ (MPa)
relative deformation ε
glass, ceramics, extremely crosslinked rubbers, polymers below Tg
metals, plastomers (in the rubbery region T)
elastomers (in the rubbery region T)

## Slide 9: Conditions of reversible deformability of elastomers
enough nodes
  knots can be chemical (cross-linking) or physical (actual crumples or crystallites)
temperature in the rubbery region
  below this temperature the elastomer behaves as a brittle material (glass region)

## Slide 10: I. Rubbers

## Slide 11: I. Rubbers
chemically cross-linked material which, within its application temperature, is capable of quickly, mostly reversibly deforming with a small force by at least 100% of its original length
otherwise they are called gums (from Latin gummi)
  these are synonyms, although other claims can be found (Do not believe them!)
it is usually made by cross-linking rubbers
  rubbers prepared from monomers other than butadiene (or derivatives) are sometimes referred to as rubbers

## Slide 12: Rubbers
usually homopolymers or copolymers of butadiene derivatives
  rubbers are created by their cross-linking
they are substances related to terpenoids, which are formed by similar reactions from a butadiene base, but often not in the form of chains
they usually have long strings
  they may not exhibit elastic properties by themselves (TPE of course does - see below)
in the undeformed state they are amorphous
they have a wide temperature range of the rubbery region, the Tg being relatively low
can be understood in two ways
  polymer that can be cross-linked to form rubber (e.g. poly(cis-isoprene))
  rubber, which is produced by cross-linking the rubber of the same name (e.g. ethylene-propylene rubber)

## Slide 13: Selected types of rubbers
rubber name | abbreviation | approximate amount (%) | utilization
butadiene styrene | SBR | 37 | general
natural | NR (natural rubber) | 32 | 
butadien | BR | 10 | 
ethylene propylene ehtylene propylene diene | EPM EPDM | 7 | 
isoprene (synthetic) | IR | 3 | 
butyl rubber | IIR | 3 | 
chloroprene | CR | 3 | oil resistant
butadiene akrylonitrile | NBR | 3 | 
akrylic | ACM | 0,5 | 
silicone | MQ | 0,1 | 
polysulfide | OT | 0,1 | heat resistant
fluorocarbon | FPM | 0,1 | 

## Slide 14: Abbreviations for rubbers (in case it was unclear)
group marking | main chain contains:
M | saturated hydrocarbon chain only
R | unsaturated hydrocarbon chain
N | nitrogen
O | oxygen
Q | siloxane groups (-Si-O-)
T | sulphur
U | nitrogen and oxygen
Z | phosphorus and nitrogen

## Slide 15: Cross-linking of rubbers - the creation of rubber
rubbers themselves usually do not have very good properties
  they tend to be sticky substances without an increased capacity for elastic deformation
  therefore it must network
cross-linking bridges form knots that prevent the chains from flowing one after the other and force them to regain approximately their original conformation (secured precisely by cross-linking)
  reactive chains (usually those with double bonds) are most often cross-linked by sulfur
    NR, BR, CR, SBR
chains with a saturated backbone can be cross-linked, for example, by peroxides (radically) or by incorporating three or more functional comonomers into their structure during production and subsequent appropriate reaction
  ethylene-propylene rubber (peroxide cross-linking)
  ethylene-propylene-diene rubber (suitable reaction on the double bond, which are here only in the side chains)
cross-linking will cause the impossibility of dissolving the given product
  they can only swell

## Slide 16: Recap.: Sulfur crosslinking of elastomers - vulcanization
the most common cross-linking reaction
  action of sulfur and heat (around 140 °C)
can be used for practically all butadiene homopolymers and copolymers
the product of elastomer vulcanization is rubber
  other additives are added to the final products (fillers, dyes, UV stabilizers, etc.)
resulting properties dependent on the amount of sulfur
  is determined in parts by weight of sulfur per hundred wt. rubber parts (phr)
    soft rubber - up to about 4 phr
    semi-hard – usually 12 to 25 phr
    hard (ebonite) – 25 to 50 phr

## Slide 17: Recap.: Sulfur crosslinking of elastomers - vulcanization
it doesn't work very well without other substances
in this case, the sulfide bridges are quite long after vulcanization (40 to 50 sulfur atoms)
  bridges on neighboring atoms and cyclic sulfide structures do not particularly help physically
  therefore accelerators and activators are used
the average number of sulfur atoms is reduced to about 1.6
  no cyclic structures or bridges are formed on neighboring atoms
activators
  ZnO, stearic acid
  accelerators
  2-mercaptobenzthiazole, tetraalkylthiuram disulfide, zinc salts of dialkyldithiocarbamates

## Slide 18: Recap.: Sulfur crosslinking of elastomers - vulcanization
probably takes place through an ionic mechanism
  observe the positive charge to understand the reaction
  the interesting thing is that both double elastomers do not participate in the cross-linking reaction, but only one - the other thus remains in the structure

## Slide 19: General rubbers - natural
natural almost pure poly(cis-isoprene)
  name perhaps from the Indian Kau-ču (weeping tree)
  obtained from latex
    aqueous dispersion of poly(cis-isoprene)
      occurs in the lactiferous cells of some plants (e.g. buttercup, swallowtail, poppy, maple, rubber tree)
  in large quantities it is obtained by cutting the bark of the Brazilian rubber tree (Hevea braziliensis)
its cross-linking creates natural rubber (gum)

## Slide 20: General rubbers - natural
trans (gutta-percha)
cis (natural rubber)

## Slide 21: Gutta-percha
natural poly(trans-isoprene)
  obtained from the latex of the Palaquium gutta tree
  its cross-linking creates gutta-percha
    it is not an elastomer but a rigid semi-crystalline polymer

## Slide 22: General rubbers - isoprene
it is basically a human attempt to copy natural rubber
  we cannot synthetically prepare poly(cis-isoprene) as pure as plants
    plants vs. human = 99.9% vs. 98%
  it is produced from isoprene by polyinsertion
    industrial production is still more expensive than natural
    depending on the purity, synthetic poly(cis-isoprene) can be mixed with natural (for a purity of around 92% from about 20%, for a purity of 96% about 50%, purer almost unlimited)

## Slide 23: General rubbers - butadiene
abbreviation BR
solution Ziegler-Natta
three different ways of binding the new monomer
  cis-1,4 (96 to 98%)
  trans-1,4 (1 to 3%)
  1,2 additions (1 to 2%)

## Slide 24: General rubbers - butadiene styrene
abbreviation SBR
production
  by radical emulsion copolymerization (decomposition of emulsifiers adds fatty or resinous acids) – statistical copolymer (rubber)
    styrene content about 20 to 25%
  solution copolymerization – high styrene SBR
    styrene content about 40 to 80%
  by ionic copolymerization - block copolymer (thermoplastic elastomer YSBR)

## Slide 25: General rubbers - ethylene propylene
abbreviation EPM
bipolymer of ethylene and propylene
Ziegler-Nattou copolymerization
resistant to degradation, but they are saturated
ethylene:propylene ratio about 3:1

## Slide 26: General rubbers - ethylene propylene diene
abbreviation EPDM
terpolymer of ethylene, propylene and some diene (for example hexa-1,4-diene)
Ziegler-Nattou copolymerization
resistant to degradation unless the main chain is saturated
  only the side chains are unsaturated and serve for cross-linking
content of diene mer around 5% (no more than 10%)

## Slide 27: General rubbers - butyl rubber
abbreviation IIR
cationic copolymerization of isobutylene and isoprene
  random copolymer
  isoprene measures mainly in trans
it can be chlorinated (CIIR) or brominated (BIIR)

## Slide 28: Oil-resistant rubbers - chloroprene
polychloroprene
  Neoprene (DuPont)
abbreviation CR
  about 85% is in the trans configuration
  it has a tendency to crystallize as a result
resistant to elevated temperatures, weather and oils
according to the temperature during synthesis they are prepared:
  fast crystallizing CR (10 °C)
    little branched, solid even without vulcanization
  medium fast crystallizing CR
  slowly crystallizing (45 °C)
for tubes, cables

## Slide 29: Oil-resistant rubbers - butadiene acrylonitrile
abbreviation NBR
  sometimes referred to as nitrile rubbers
statistical bipolymer
according to the content of acrylonitrile mers
  with low content (18 to 26%)
  with medium content (30 to 35%)
  with a high content (40 to 50%)
oil resistant

## Slide 30: Oil-resistant rubbers - polysulphide
many advantages
  excellent oil resistance
  partially resistant to even slightly polar solvents
  they swell little
  chemically resistant (do not contain double bonds) - weather resistance
  low gas permeability
they have only a small drawback
  when heated it bursts with sulphur
    if you want to play devils, definitely consider it an advantage
y

## Slide 31: Heat-resistant rubbers - silicone
these are linear siloxanes
wide temperature range of the rubbery region
  due to low chain cohesion
    but also worse physical properties because of this
heat resistant
peroxides can be cross-linked, for example
adhesive materials (insulating tapes), mastics, glues, rubbers are made from them
  in addition to silicone polymers, the tube also contains methyltriacetosilane, which functions as a crosslinker (anionic reaction initiated by air humidity)

## Slide 32: Heat-resistant rubbers - silicone
polydimethoxysiloxane
(MQ)
methylvinylpolysiloxane
(MVQ)
methylfenylvinylpolysiloxane
(MPVQ)
methyltrifluorpropylvinylpolysiloxane
(MPQ)

## Slide 33: Heat-resistant rubbers - fluorocarbon
Rambo among rubbers
  withstands the highest temperatures among rubbers (over 200 °C)
  rubbery area already from about -25 °C
  resistant to oils
  resistant to acids (concentrated sulfuric, nitric, etc.)
  resistant vapors
  resistant to oxidation (weathering)
this is why they are some of the most expensive

## Slide 34: Heat-resistant rubbers - fluorocarbon
they are usually copolymers of vinylidene fluoride and other comonomers:
  tetrafluoroethylene
  hexafluoropropylene
  hydroxypentafluoropropylene
  etc.

## Slide 35: Additives in rubbers
most common isoprene or diene rubbers
  therefore, they contain double bonds that are relatively reactive
  are susceptible to degradation
  it must be doped with anti-degradation substances
rubbers with a saturated chain are usually quite stable and thus do not need anti-degradation agents
  e.g. ethylene-propylene rubbers

## Slide 36: II. Termoplastické elastomery

## Slide 37: Termoplastické elastomery
TPE
definition
  general:
    a group of chemically non-cross-linked heterogeneous substances capable of significant reversible deformation under the application of low voltage and an amorphous structure in the undeformed state
  specific:
    thermoplastic copolymers consisting of immiscible flexible (elastic) and rigid (rigid) segments resulting in an elastic material (like rubber) that can be recycled (like thermoplastics)
    this is how thermoplastic elastomers are more often understood
elasticity given by physical knots (so they are not networked) and entropy

## Slide 38: Thermoplastic elastomers
segments
  flexible
    rubbery in a wide temperature range
    they add flexibility to the material
  stiff
    glassy or highly crystalline at the temperature conditions of use
    they limit the mutual mobility of the chains and fulfill the function of nodes
    thanks to the absence of a chemical bond, they enable the material to be recycled

## Slide 39: Types of thermoplastic elastomers
blocky
  usually by ionic (living) polymerization
polycondensation
  polyurethanes
  polyetheresters
  polyetheramides
mixed polymers
  mixing molten elastomers with thermoplastics
  sometimes a sparse network is formed due to shear stress
    at that moment they are on the borderline of thermoplastic elastomer and sparsely cross-linked rubber

## Slide 40
group | subgroup | flexible (soft) segment | rigid (hard) segment | structure | 
block |  | -butadiene- | -styrene- | -styrene-butadiene-styrene- | 
 |  | -isoprene- | -styrene- | -styrene-isoprene-styrene- | 
 |  | -ethylene-propylene- | -styrene- | -styrene-ethylene-propylene-styrene- | 
 |  | -ethylene-butylene- | -styrene- | -styrene-ethylene-butylene-styrene- | 
 |  | -ester- | -styrene- | -styrene-estere-styrene- | 
 |  | -amide- | -styrene- | -styrene-amide-styrene- | 
polycondensated | polyuretany | -ether- or -ester- | -uretane- or -urea- | -uretane-ether-uretane- or -urea-ester-urea- | 
 | polyetherestery | -ether- | -ester- | -ester-ether-ester- | 
 | polyetheramidy | -ether- | -amide- | -amide-ether-amide- | 
mixed |  | -elastomeric- | -thermoplastic- |  | 

## Slide 41: Ionomers
crosslinking bonds are not covalent but ionic (or hydrogen)
  it is thus in a way a rubber whose crosslinks can be relatively easily split and then restored again (something between rubber and thermoplastic rubber)
copolymer of ethene and 5-10% acrylic or methacrylic acid
  carboxyl groups can be neutralized to form an acrylate or methacrylate salt (Na, Ca, Mg, Zn, Al, Ba)
  it is not a static network and monovalent ions (Na) contribute to its strength
with enough temperature I can disrupt the network without degrading the macromolecules themselves
  can be melted and after cooling I get the network again
physically they behave similarly to thermoplastic elastomers

## Slide 42: Thank you for your attention