## Slide 1
Inovace stávajících nebo tvorba nových metodických a elektronických studijních materiálů v ČJ nebo AJ
Ing. Pavel Holec
Nové možnosti rozvoje vzdělávání na Technické univerzitě v Liberci
Specifický cíl A2: Rozvoj v oblasti distanční výuky, online výuky a blended learning
NPO_TUL_MSMT-16598/2022

## Slide 2: Polymer solutions

## Slide 3: 1. Dispersions

## Slide 4: Dispersion - basic terms
dispersion system
  generally a mixture of at least two phases
  the dispersion fraction dispersed in the dispersion medium
degree of dispersion
  describes the particle size of the dispersed phase
  inverse of the particle size of the dispersion fraction
the shape of the particles of the dispersion fraction
  isometric
    similar in all three dimensions (e.g. spherical)
  anisometric
    flattened (plates, lamellae), elongated (rods, fibers)
  the shape of the molecules can change

## Slide 5: the dispersion fraction the dispersion medium

## Slide 7: Dispersions according to the degree of dispersity
true solutions of low molecular weight substances
coloidal
(1 – 1000 nm)*
micellar and macromolecular solutions
analytical
(<1 nm)
dispersion
coarse
(> 1000 nm)
suspensions, emulsions, foams, dust, smoke etc.
* není pevná hranice

## Slide 8: 2. Thermal movements of the dispersion fraction

## Slide 9: Thermal movement of the particles of the dispersion fraction
oscillation of atomic nuclei around equilibrium positions
accidental collision of molecules of the dispersion medium into the particles of the dispersion portion due to the influence of heat
  due to randomness, it is necessary to investigate statistically
types of the movements
  vibratory
  translational
  rotational
  internal (intramolecular) rotation
    in macromolecules

## Slide 10: Vibrational movements
movements of the nuclei of the atoms of the molecule relative to the center of gravity of the molecule
* visualization of vibrational movements: https://en.wikipedia.org/wiki/Molecular vibration

## Slide 11: Vibrational motion – valence deformation
the atoms oscillate with respect to the center of gravity of the molecule
  in the animation, the hydrogen atom is static and the chlorine atom is moving
    in fact, the lighter hydrogen atom vibrates more
the higher the temperature, the greater the movement path
* vibrational model of HCl : https://en.wikipedia.org/wiki/File:Anharmonic_oscillator.gif
D0 … dissociation energy

## Slide 12: Brownian motion
disordered movement of small particles in a liquid observed in 1827 by the botanist Robert Brown
  pollen grains of the sculpin (Clarkia pulchella) in water
    size of pollen grains approximately 1 μm
    later he also tried the pollen grains of other plants
  at first he believed that the living substance of the pollen was responsible for the movement, but after experiments with inanimate particles he disproved it himself
  the smaller the particles he used, the more vivid the movement he observed

## Slide 13: Brownian motion - model
* molecular model of Brownian motion: https://youtu.be/6VdMp46ZIL8

## Slide 14: Brownian motion - fact
* real observation of Brownian motion (with extremely moving music, so you better turn off the sound for a moment): https://www.youtube.com/watch?v=R5t-oA796to

## Slide 15: Translational thermal motion
causes equalization of concentrations in the system (given by the concentration gradient)
diffusion
  the movement of particles of the dispersion fraction into an environment with a lower concentration
osmosis
  the movement of molecules of the dispersion medium into an environment with a higher concentration of particles of the dispersion fraction
  through a semipermeable (semipermeable) membrane
    it only passes the dispersion medium, it captures the dispersion part

## Slide 16: Diffusion
the movement of particles of the dispersion fraction into an environment with a lower concentration
dispersion fraction
dispersion medium
concentration imbalance
concentration equilibrium

## Slide 17: Osmosis
movement of particles of the dispersion medium into an environment with a higher concentration of particles of the dispersion portion
concentration imbalance
concentration equilibrium
semipermeable membrane

## Slide 18: Osmotic pressure
osmotic pressure π:
R … relative gas constant (8.314 J·K-1 ·mol-1)
T ... thermodynamic temperature [K]
V … system volume [m3]
and … solvent activity (describes the degree of interaction of the fluid with its environment)
for a highly dilute solution:
n ... substance amount of solvent [mol]
c … molar concentration·[mol·dm-3]

## Slide 19: Osmometry
determination of osmotic pressure π:
ρ … solvent density
h ... the difference in the heights of the levels
g … gravitational acceleration

## Slide 20: 2. Solubility of polymers
Similia similibus solvuntur.

## Slide 21: Macromolecules in solution
concentration of macromolecules in solution
flexible chains
rigide chains

## Slide 22: Shapes of macromolecules in solution
globules
  tightly coiled polymer chains
  interaction with the solvent only on the surface of the globule
  chemical or physical bonds ensure a more permanent shape of the globule
coil
  not very tightly coiled polymer chains
  polymer chains interact with other chains and with solvent molecules
unfolded chains
  the polymer chain interacts almost exclusively with solvent molecules (good soln.)

## Slide 23: Basic thermodynamic quantities
Gibbs (free) energy G
  the basic condition for the spontaneity of the plot
  ΔG < 0 says that the action can be spontaneous (at constant temperature and pressure)
  as a state quantity, it considers only the initial and final state, not the progress
    due to e.g. an energy barrier, the event may not occur spontaneously, even though ΔG < 0 applies to it
enthalpy H
transferred energy (heat) at constant pressure
  exothermic reaction (ΔH < 0) – energy leaves the system
  endothermic reaction (ΔH > 0) – energy enriches the system
entropy S
  degree of system disorder (the larger, the more disordered)
  for mixing it must practically always increase (i.e. be positive)
    thus, the change in Gybbs energy during mixing is mainly influenced by the change in enthalpy

## Slide 24: Gibbs free energy
the possibility of self-mixing of the solvent assumes ΔG < 0
surrounding
system

## Slide 25: Solvent lattice model
a two-dimensional mixture of two components at grid nodes
  does not contain blank spaces
  each node is occupied by exactly one segment
  after mixing, the total volume does not change
  the volume of one segment of solvent equal to the volume of one molecule* of solvent
coordination number of
  the number of interactions of one segment with others
  z = 4 in our case
segment interaction
  their total number does not change, only the "links" between them
types of mutual interactions of segments in a two-dimensional grid
  polymer-polymer
  polymer-solvent
  solvent-solvent
* in the case of the lattice model, the term segment will be used for the volume unit in the lattice, whether it is a polymer or a solvent

## Slide 26: Enthalpy of a two-component mixture
the change in enthalpy of mixing ΔHm corresponds to the energy change Δε of all new bonds (their total number is l) polymer-solvent
bond energy change Δε upon mixing
  given by the sum of changes in polymer-polymer (εpp), polymer-solvent (εpr) and solvent-solvent (εrr) interaction energies
  if 1 εpp and 1 εrr disappear, 2 εpr bonds can be formed by mixing
εPP = εpp
εSS = εrr
εPS = εpr

## Slide 27: Enthalpy of mixing
the total number of polymer-solvent interactions l is given by:
  the probability of the occurrence of a solvent in the vicinity of a given polymer segment
    it is represented by the solvent volume fraction ϕr (small phi)
  by the coordination number z (number of neighbors of each segment)
  by the number of polymer segments Np
    the number of Np segments can be calculated using Avogadro's constant NA and the molar amount of polymer segments np
  so overal:
the change in enthalpy of mixing ΔH corresponds to the energy change Δε of all new polymer-solvent bonds
then:

## Slide 28: Hildebrand-Scott solubility parameter
is denoted by δ (small delta)
sometimes also called the total solubility parameter
  where CED is the cohesive energy density, ΔvHm is the molar vapor enthalpy change, p is the pressure, ΔV is the volume change, and Vm is the molar volume
CED
  describes the mutual cohesion of the molecules of the given substance, or the total energy of its secondary bonds (therefore we do not consider gases)
  defined as the internal vapor energy Uv of a unit volume of liquid Vm
  increases with the polarity of the substance

## Slide 29: Hildebrand-Scott solubility parameter
substances with similar δ tend to be miscible
for a mixture of several substances, the resulting δ is equal to the weighted (according to their volumes) average of the parameters of the mixed substances

## Slide 30: Determination of δ of polymers
I am not able to evaporate polymers without their decomposition
  it is not possible to determine CED by the usual method
non-solvent precipitation
  dissolve the polymer in the right solvent and titrate with the non-solvent
  at the moment of precipitation, we determine the δ of the polymer
swelling in solvent
  we soak the cross-linked polymer in solvents of different δ values
  in which it swells the most, we assign such a δ to the polymer

## Slide 31: Disadvantages of the Hildebrand parameter
for some substances, discrepancies appeared between the theoretical (calculated) value of the Hildebrand solubility parameters and the experimentally determined value
The Hildebrand parameter describes the contribution of all secondary bonds
  it would be more appropriate to consider individual contributions separately
  three contributors
    dispersion forces
    polar forces
    hydrogen bonds
growth of bond strength

## Slide 32: Hansen parameters
splitting the Hildebrand (total) solubility parameter δ into three partial solubility parameters:
  dispersion forces δd
  polar forces δp
  hydrogen bonds δh
  unit is
ionic interactions are not considered
they are determined experimentally and by calculation

## Slide 33: Dispersion (London) forces
generally the weakest of the physical forces
  they decrease with the 6th power of the distance (so they act over a short distance)
temporary weak dipoles
  they arise due to short-term random changes in the electron density in the atomic shell
    a consequence of the imaginary movement of electrons in the shell
  they can induce a similar change in neighboring atoms
their number increases with the size of the surface of the molecule
  straightened chains therefore a greater number than coiled

## Slide 34: Polar interactions
permanent dipoles
  they arise due to a permanent imbalance of the electron density distribution in the molecule
  a consequence of the different electronegativities of the atoms in the molecule
non-polar molecule
(does not form a permanent dipole)
polar molecule
(forms a permanent dipole)

## Slide 35: Hydrogen bridges
the strongest of physical forces
  basically a special case of polar interaction
permanent dipole
  hydrogen bonded to a very electronegative element (F, O, N)
    hydrogen bond strength given by the structure
  the hydrogen electron is attracted to the more electronegative atom so much that the hydrogen nucleus (proton) is practically exposed
  allows interaction with a neighboring dipole to form a "proton bridge"

## Slide 36: Solubility ball
plotting Hansen's parameters in a three-dimensional graph
  unfortunately, the dispersion forces are so small that the ball usually does not come out
    the dispersion forces parameter δd is therefore multiplied by 2
the center of the sphere corresponds to the parameters of the solute
for each substance there is the largest radius R0 of the solubility sphere, for which it is valid that if the solvent lies in the solubility sphere, it dissolves the given substance
  we call R0 the interaction radius
  V ... is the distance of the solvent position from the center of the sphere

## Slide 37: 2D graphs of Hansen parameters
plotting two Hansen parameters in a two-dimensional graph
  rectangular projection of the 3D graph into one of the planes given by the coordinate axes (one parameter constant)
δP
δD
δP
δH
δD
δH

## Slide 38: 2D graphs of Hansen parameters
plotting two Hansen parameters in a two-dimensional graph
  rectangular projection of the 3D graph into one of the planes given by the coordinate axes (one parameter constant)

## Slide 39: Teas (triangle) charts
the solubility sphere is difficult to work with in a two-dimensional display
practice often uses triangular charts
  individual parameters are relativized
the graphs describe only the mutual proportion of individual solubility parameters
  it appears as if all fouling substances have the same absolute value of the Hildebrand parameter
  they are not completely accurate, but they are usually sufficient for practice

## Slide 40: Teas (triangle) charts
fD = 0,4
fP = 0,4
fH = 0,2

## Slide 41: Good and bad solvents
ideal solvents
good solvents
bad solvents

## Slide 42: Teas (triangle) charts
for the mixture it is again true that the resulting f is equal to the weighted average of the relative parameters of the mixed substances
in this way, a good solvent can be prepared from several bad solvents (so-called cosolvency)
3 vol. part of A
1 vol. part of B
we want to dissolve this, but we only have the not-so-suitable solvents A and B

## Slide 43: Solubility of polymers
we consider a binary polymer-solvent mixture
  In this case, the polymer is monodisperse (polydisperse systems are understandably more complicated)
different for amorphous and semi-crystalline polymer
dependent on solvent, polymer, temperature, pressure, etc.

## Slide 44: Effect of molar mass on solubility
the critical concentration decreases with increasing molar mass
  r = the volume fraction of the macromolecule segment to the unit volume of the solvent (these segments do not generally correspond to monomeric units)

## Slide 45: Dissolution of semicrystalline polymers
crystalline parts less soluble
  the solvent must overcome the physical bonds between the macromolecular chains

## Slide 46: Dissolution of semicrystalline polymers
can be conceptually divided into two parts
  crystallite dissolution
    The Gibbs energy due to the disappearance of crystallites (below their melting temperature) increases and must be compensated (reduced) by the Gibbs energy of mixing
      however, it needs a significant excess of solvent and a sufficient temperature
    semicrystalline polymers can thus be of limited solubility
  dissolution of the amorphous polymer
solubility of semicrystalline PE depending on temperature (ϕ2r is the maximum soluble volume fraction of the polymer in the solution)

## Slide 47: Conductivity of the polymer solution
concentration [mol·l-1]
el. conductivity [mS·cm-1]
viscosity [mPa·s]

## Slide 48: Entanglements
cohesive entanglements
physical entanglements (knots)

## Slide 49: 4. Polymer solutions for electrospinning

## Slide 50: Electric spinning
polymer solution or melt
direct current (DC) or alternating voltage (AC)
  combinations also possible (e.g. DC + centrifugal)
needle, rod, roller, disc, string, other
elongation and orientation of macromolecules (from solution or melt) induced by strong el. field

## Slide 51: Process parameters of spinning
electrode
collector
electric field strength
temperature
humidity
the duration of the electric field
solution flow rate

## Slide 52: Geometry of spinning

## Slide 53: Electrospinning system parameters
polymer
  molecular weight
  concentration
solvents
  permittivity
  volatility
  surface tension
  electric conductivity
viscosity

## Slide 54: Surface tension of solvents
the molecules of the liquid have a higher affinity to each other than to the molecules of the surrounding gas
  surface tension where liquid and gas molecules meet
acts against the electric voltage
  preventing the formation of a cone
  excessive surface tension → does not thread, spray or drip defects on the threads

## Slide 55: Permittivity of solvents
measure of resistance to polarization of the dielectric
  ε (small epsilon)
  units of F·m-1
generally the higher the better
  more uniform charge distribution on the surface of the solution
  higher productivity, lower fiber diameters

## Slide 56: Volatility of solvents
evaporation rates (under given conditions)
ideally, all solvent should evaporate before depositing on the collector
  otherwise there is a risk of reverse dissolution
  too much volatility causes the fibers to solidify before reaching nanoscale
standard fibers
back dissolved fibers

## Slide 57: Zapleteniny
předpoklad dobrého zvlákňování
  přechod mezi sprejováním a zvlákňováním
závislé na rozpouštědlech, polymeru, molární hmotnosti, koncentraci

## Slide 58: Thank you for your attention