## Slide 1
Inovace stávajících nebo tvorba nových metodických a elektronických studijních materiálů v ČJ nebo AJ
Ing. Pavel Holec
Nové možnosti rozvoje vzdělávání na Technické univerzitě v Liberci
Specifický cíl A2: Rozvoj v oblasti distanční výuky, online výuky a blended learning
NPO_TUL_MSMT-16598/2022

## Slide 2: Polymer melts

## Slide 3: Polymer melts
polymer in liquid state
  only non-crosslinked polymers with Tdegradation higher than Tf
    more densely cross-linked rubbers cannot be melted
    PAN is not cross-linked, but degrades before it melts (has Tdegradation < Tf)
above the flow temperature Tf
  intermolecular secondary bonds disappeared due to thermal motions
  macromolecules slide and flow over each other

## Slide 4: Flow properties of polymer melts
creep resistance (viscosity) of polymer melts dependent on many factors:
  temperature
  molecular weight
  molecular weight distribution
  additives
  creep rate
  creep time
are generally referred to as non-Newtonian fluids (more generally fluids)

## Slide 5: Viscosity model
the investigated fluid is closed between the static pad and the upper plate of surface A moving due to the force F
the fluid moves together with the upper plate
we divide the fluid into imaginary layers (flow channels)
  the layer closest to the static substrate practically does not move
  the layer closest to the top plate moves the most

## Slide 6: Newton's law of viscosity
flow properties are expressed by the so-called shear (tangential) stress σ (small sigma)
  sometimes also marked τ (small tau)
  its negative value is often given because it acts against the direction of the force F
  σ … shear stress [Pa]
  F ... force acting on the top plate [N]
  A … plate area [m2]
  η … dynamic viscosity [Pa·s-1]
  𝛾 ̇ … velocity gradient (shear velocity gradient) [s-1]
γ … rate of shear deformation (describes the relative displacement of the layers, therefore dimensionless) t ... time [s]

## Slide 7: Attention!
some texts consider the value described in the figure by the number du differently:
  displacement of parallel surfaces
    dimension is [m] and then:
  shift speed change
    dimension is [m·s-1] and then:
therefore, in some texts, Newton's law appears in one of the following forms:

## Slide 8: Viscosity
describes the degree of internal friction of the liquid and thus the resistance to creep
  it is the cohesive forces between the streamlines that slow down the flow
generally depends on
  temperature
  concentration and molecular size
different types of viscosities*
  dynamic
  kinematic
  relative
  reduced

## Slide 9: Newtonian fluids
they behave according to Newton's law
  the strain rate is directly proportional to the shear stress
  viscosity is a proportionality constant
    it does not change with strain rate, shear stress, or its duration
    is temperature dependent

## Slide 10: Non-Newtonian fluids
eg polymer solutions and polymer melts
viscosity is not constant
they generally behave according to an equation strikingly similar to Newton's equation
however, instead of the dynamic viscosity η, it uses the apparent viscosity ηz (sometimes also ηa)
  this is dependent on temperature (just like Newtonian fluids)
  further dependent on the rate of deformation, the shear stress or the time of its action

## Slide 11: Apparent viscosity ηz
temperature dependent a
  shear rates
    pseudoplastic liquids
    dilatant liquids
  during shear stress
    thixotropic liquids
    reopex liquids
  shows a flow limit
    Bingham liquids

## Slide 12: Pseudoplastic liquids
the apparent viscosity decreases rapidly with increasing tangential stress
  the more I strain, the better it flows
reduction of viscosity caused by the orientation of anisometric particles in the direction of movement of the liquid
e.g. usual polymer solutions and their melts
  generally applies to dispersions with an anisometric dispersion fraction
technologically usually advantageous

## Slide 13: Pseudoplastic liquids
Newtonian fluids

## Slide 14: Dilatant liquids
the apparent viscosity increases rapidly with increasing tangential stress
  the more I strain, the worse it flows
in a concentrated suspension at rest, the particles are surrounded by a small layer of liquid (which acts as a lubricant and thus allows flow) and occupy the smallest possible volume (they fit together as best as possible)
  however, during shear stress, the particles move from their ideal position, increase their volume, and the liquid is no longer sufficient to wet them
  if the rate of shear stress is too high, it is not enough for the liquid to reach all the particles and this will significantly increase the internal friction in the liquid (i.e. viscosity)
observed for concentrated suspensions (e.g. polymer suspensions, concretes, etc.)
technologically disadvantageous

## Slide 15: Thixotropic and rheopex liquids
thixotropic liquid
  the apparent viscosity decreases with the duration of the shear stress
  the longer I strain, the better it flows
  a reason similar to that of pseudoplastic liquids, but the arrangement of anisometric particles occurs with a considerable delay
  technologically advantageous
    especially for mixing or painting
reopex liquids
  the apparent viscosity increases with the duration of shear stress
  the longer I strain, the worse it flows
  the reason is similar to that of dilatant liquids, but dilation occurs with a significant delay
  technologically disadvantageous

## Slide 16: Bingham liquids
they show significant flow properties only after exceeding the so-called (dynamic) flow (or yield) limit σt
  they may behave Newtonian or non-Newtonian when the flow limit is exceeded
the flow limit represents the stress that is needed to overcome the attractive forces between the dispersed particles
usually mushy or pasty suspensions or gels (chalk, toothpaste, lime)

## Slide 17: Newtonian and non-Newtonian fluids
1 – Newtonian, 2 – pseudoplastic, 3 – dilatant, 4 – Bingham non-Newtonian, 5 – Bingham Newtonian

## Slide 18: Effect of molecular weight distribution
the wider the distribution, the earlier non-Newtonian behavior appears
frequency

## Slide 19: Siphon effect
during pouring, the melt or solution pulls itself from one container to another even after e.g. water would not be able to flow
given by physical nodes and secondary bonds between chains
  requires a sufficiently high molecular weight

## Slide 20: Weissenberg phenomenon
pushing a non-Newtonian fluid towards a rotating body
  manifestation of the elasticity of liquids
  generation of stress perpendicular to the surface of the rotating body
it can be simply imagined that long macromolecules wind up on a rotating body and pull others
newtonské
nenewtonské

## Slide 21: Increase in profile behind the nozzle
tension is released, when the melt "springs" in free space
it limits production speed

## Slide 22: Rotational viscometry / rheology
relative method
the torsional stress sensor senses the force, proportional to the resistance exerted by the examined fluid
many geometric arrangements of measuring instruments:

## Slide 23: Melt flow index
melt flow rate (MFR)
an important parameter for mass production
it describes the real behavior of the melt without having to investigate the chemical-physical parameters in a complicated way
important e.g. for meltblown or spunlace technology
corresponds to the amount (weight, volume) of polymer melt at a defined temperature flowing through a defined nozzle at a defined pressure for a period of 10 minutes
  units therefore g/(10 min) or ml/(10 min)
is measured with an extrusion plastometer

## Slide 24: Scheme of the extrusion plastometer

## Slide 25: Processing of polymer melts
compared to solutions, melts have a fundamental:
  advantage – these are cleaner polymers (no solvent, etc.)
  disadvantage - I have to heat it up a lot, which is expensive
processing methods
  extrusion
  injection
  blowing
  thermal-vacuum forming of foils
  calendering
  pressing
  fiber production

## Slide 26: Injection molding
a granulate of polymer or polymers is poured into the hopper
the auger transports the granulate to the compression zone, where it is wetted and the heating elements heat and melt it
further, the screw conveys the melt to the extrusion head
the result depends on further processing
  injection
  indebtedness
  cooling and back granulation
  etc.

## Slide 27: Injection molding
first identical to extrusion, but the extrusion head leads through a narrow neck into the mold

## Slide 28: Injection Blow Molding
classic: production of hollow products
extrusion blow molding: film production
  the blown bubble is pressed between the rollers onto the foil

## Slide 29: Thank you for your attention