## Slide 1
Inovace stávajících nebo tvorba nových metodických a elektronických studijních materiálů v ČJ nebo AJ
Ing. Pavel Holec
Nové možnosti rozvoje vzdělávání na Technické univerzitě v Liberci
Specifický cíl A2: Rozvoj v oblasti distanční výuky, online výuky a blended learning
NPO_TUL_MSMT-16598/2022

## Slide 2: Additives in polymers

## Slide 3: Additives in polymers
they modify the properties of the polymer product
together with macromolecules they form polymer mixtures
their amount in the polymer is given in unit phr
  phr (weight parts per hundred of rubber)
in total, it is possible to add more than 100 phr (but it depends on the polymer)
types of ingredients
  processing
  antidegradants
  mesh
  affecting other physical properties
  strange

## Slide 4
Additives in polymers
processing
antidegradants
cross-linking
crosslinking agents
processing plasticizers
others
fillers
special
lubricants
separators
auxiliary ingredients
thermal stabilizers
light antidegradants
antioxidants
antiozonants
activators
accelerators
reinforcement
puffing additives
optical brighteners
antistatic
adhesives
flame retardants
abrasives
explosives and fuels
sulfur and its derivatives
peroxides
energy-rich radiation
vulcanization activators
peroxide activators
vulcanization accelerators
curing accelerators
plasticizers
plasticizers

## Slide 5: Processing additives
are added to facilitate the processing of the polymer
  their primary purpose is therefore not to influence the resulting properties of the product, but they still do so to a certain extent
types:
  processing plasticizers
  lubricants
  separators
  plasticizers
  thermal stabilizers
  other processing ingredients

## Slide 6: Processing plasticizers
used in the plasticization (kneading) of rubbers (but sometimes also with thermoplastics)
  a process in which the macromolecules of the rubber are mechanically torn apart and re-linked
  unification of molecular weights
  preparation of rubber compounds
otherwise also peptizers
  they facilitate kneading
  they stabilize the radicals formed
  accelerate plasticization
also when recycling rubber into so-called regenerated material
  it is about tearing the original cross-linked macromolecules so that the result is reprocessable and vulcanizable
  moss. the properties of the regenerate are always lower than those of the original macromolecules (molecular weights are lower)
around 0.05 phr are added for plasticization, up to about 4 phr for regeneration
Peptazine BAFD
Peptazine BFT

## Slide 7: Lubricants
internal lubricants
  rather soluble in the polymer
  reduce melt viscosity and friction (easier processing)
external lubricants
  rather insoluble in the polymer
  forms a separation layer on the surface of the polymer
    the polymer then does not stick to surrounding products or equipment
    protects the polymer from weathering
    unifies the look
the lubricant is never internal only or internal only
types of lubricants according to chemical composition
  liquid or solid alkanes (paraffinic oils and paraffins)
  fatty acids, their salts (calcium), esters or amides
  waxes (natural and synthetic)
  heavy alcohols (more than 30 carbons)
  polyhydric alcohols
combination of the previous ones
dosage usually from 0.5 to 3 phr

## Slide 8: Separators
forms a layer preventing the product from sticking to the device
coatings or spraying of mold surfaces
  must withstand high temperatures
  silicone oils, PTFE dispersion
  they are difficult to remove and limit subsequent surface treatment of the product (e.g. dyeing [ideally green])
separation foil
  easier separation from the product
  cellophane, PVA

## Slide 9: Other processing additives (rubber)
reduce the viscosity of the rubber mixture during mixing (with fillers, etc.)
  they increase the possible processing speed of the mixture without degradation of macromolecules due to shear stresses
  they reduce frictional heat during mixing of the mixture
two kinds
  fatty acids and their salts (Ca2+, Zn2+)
  resin
dosage up to 10 phr

## Slide 10: Plasticizers
they reduce the Tg of the product
  they get between the macromolecules and artificially create a space that allows the segmental movements of the macromolecules
  the plasticizer must therefore be a solvent of the given polymer (so that it can penetrate between the macromolecules and distance them from each other)
usually organic substances
  they should not leak out of the product, but phthalates in PVC, for example, do not do this very well (they cause a distinctive smell of new linen)
types
  non-polar plasticizers
    for non-polar and slightly polar polymers
    oils, tars
  polar plasticizers
    for polar polymers
    phthalates, adipates, sebacates of higher alcohols
  macromolecular
    they do not volatilize, but have lower efficiency
    PEG, PES, resin
voda jako (těkavé) změkčovadlo bavlny

## Slide 11: Thermal stabilizers
prevent or at least limit the thermal degradation of macromolecules during processing (mainly for PVC)
two main tasks
  prevent the splitting off of low molecular weight substances from the polymer (e.g. HCl)
  they prevent the formation of colored structures
two kinds
  inorganic or organic salts and their suitable mixtures
    some salt mixtures increase the stabilization effect (synergy), while others reduce it
  organic substances (epoxides, esters)
dosage around 0.5 to 5 phr

## Slide 12: Antidegradants

## Slide 13: Antidegradants
protects the polymer from environmental influences (air oxygen, sunlight)
types
  light stabilizers
  antioxidants
  antiozonants
dosage between 1 and 3 phr

## Slide 14: Light stabilizers
usually UV stabilizers
  UV is energetically rich enough to break chemical bonds
  visible radiation does not matter so much
properties
  they absorb UV radiation and convert it into energy-poor radiation that does not damage the polymer as much
  they do not decompose themselves due to UV (they only act as catalysts)
  do not react with the polymer (even during UV catalysis)
examples
  hydroxy (-OH) or alkoxy (-OR) derivatives of benzophenone
  salicylic acid derivatives
  benzotriazole derivatives
  sterically shielded amines (HALS = hindered amine light stabilizer)
  inorganic salts TiO2 and ZnO or carbon black
benzofenone
salicylic acid
benzotriazole

## Slide 15: Antioxidants
they limit the action of atmospheric oxygen
reactions of the polymer with oxygen usually take place slowly, but when heated or exposed to radiation they are greatly accelerated
particularly susceptible to unsaturated structures
under the influence of oxygen, radicals and cross-linking occur, which results in brittleness of the product
  the O2 molecule binds to the structure to form hydroperoxide –OOH, when the peroxide bond is then homolytically split to form radicals
  radicals cause chain reactions (reaction products further react with the polymer)
mechanism of inhibition of chain reactions
  preventing the formation of a radical
  breaking the chain reaction

## Slide 16: Antioxidants
antioxidants do not always act as catalysts and reactions with oxygen or its reaction products may result in altered
  these products may be colorless or colored (which is undesirable)
non-dyes include phenol and cresol derivatives:

## Slide 17: Antiozonants
ozone reacts readily with double bonds in rubber
  a hard inelastic layer is formed on the surface of the rubber
  due to fragility, this layer cracks, resulting in a fresh surface
  the new surface is exposed to new ozone and finally there is a total loss of the useful properties of the rubber
they only work on the surface of the product (where there is ozone)
as well as antioxidants can color the polymer after reaction
  the most effective, but coloring, are p-phenylenediamine derivatives
waxes or paraffins are also used (they form a barrier against ozone)
saturated rubbers are not very susceptible to ozone

## Slide 18: Cross-linking agents

## Slide 19: Cross-linking agents
are added to crosslink polymers and oligomers
types:
  crosslinkers (crosslinking agents)
  crosslinking activators
  crosslinking accelerators

## Slide 20: Crosslinkers (crosslinking agents)
the aim is to create a product that is stronger, harder or more stable in shape and heat
different designations according to the material we mesh
  vulcanizing agents (cross-linking rubbers)
  hardeners (cross-linking reactoplasts)
  thermoplastics can also be crosslinked, but their crosslinkers do not have a special designation
crosslinking of thermoplastics
  organic peroxides
  high-energy radiation (obviously not an additive)
    γ radiation (cobalt emitters)
    electron beams
    UV

## Slide 21: Crosslinkers - vulcanizing agents
rubber cross-linking agents (vulcanization takes place at higher temperatures)
the most common is sulfur
  for unsaturated rubbers
  two kinds
    crystalline (eight-membered rings)
    polymeric (long chains)
      at elevated temperature, the chains split and the rubber cross-links
    organic disulfides or polysulfides (so-called sulfur donors)
sulfur dosing
  soft rubber from 0.5 to 4 phr
  hard rubber 35 to 50 phr
sometimes an addition of 0.5 phr Se or Te to increase heat resistance
  dosing of sulfur donors
    up to 4 phr

## Slide 22: Crosslinkers – (vulcanizing) agents
organic peroxides
  can cross-link saturated (as well as unsaturated) rubbers
  dosage in phr units (but in diluted form)
  dangerous spontaneous combustion and explosion
dicumyl peroxide
dibenzoyl peroxide
2,4-dichlordibenzoyl peroxide
2,5-dimethyl-2,5-di(t-butylperoxy)hexane

## Slide 23: Síťovadla – vytvrzovací činidla
cross-linking reactoplasts
acid
  harden aminoplasts and resols (phenoplasts)
  acid condensation of methylol groups
    resins are thus created from resols
nitrogenous substances
  hexamethylenetetramine
  hardens novolacs (acids do not work on them)
  condensation with the release of ammonia (NH3) and the formation of methylene bridges
    polyamines
    polyaminoamides
thiols and thioacids (sulphur-containing substances)
peroxides (see previous)
dosage
  depending on the reagent used
  usually up to 10 phr
hexamethylentetraamine
polyamine
polyaminamide
dithiol(ester)

## Slide 24: Crosslinking activators
catalyze cross-linking reactions (reduce their activation energy)
  more homogeneous cross-linking
  more effective cross-linking (need to add less cross-linking agent)
they are divided according to crosslinking agents
  vulcanization activators
  peroxide activators
  sensitizers (activators of radiation cross-linking)

## Slide 25: Vulcanization activator
inorganic oxides dissolved in fatty acids
  acid (0.5 to 3 phr) is used to dissolve the oxide in the rubber
    stearic (18 carbons), lauric (12 carbons), 2-ethylcapronic (2+6 carbons)
  ZnO
    dosage about 3 phr
  CdO
    it is limited due to health problems
  PbO
    it has one advantage – it activates well
    it has many disadvantages
      poisonous
      expensive
      black rubber during vulcanization (formation of PbS)

## Slide 26: Peroxide activators
multifunctional molecules, partially stabilizing radicals
  sometimes they are crosslinkers and activators in one
  triallyl cyanurane (TAC), triallyl isocyanurane (TAIC)
  dicarboxylic acid esters
  methacrylate derivatives
increase networking efficiency by up to 20%
  after the breakdown of peroxides, the radicals preferentially react with the activator, which subsequently cross-links
sometimes they also serve as stiffeners
dosing up to 5 phr
TAC
TAIC

## Slide 27: Sensitizing activators
radiation activators
again dicarboxylic acid esters or structures with conjugated systems capable of stabilizing radicals
they work similarly to peroxide activators, but their main goal is to prevent degradation reactions of macromolecules due to radiation

## Slide 28: Networking accelerators
speed up cross-linking reactions (from hours to minutes)
  they reduce the amount of crosslinker needed
  they reduce the necessary vulcanization temperature
  enabled continuous vulcanization (the product goes along the line and is continuously vulcanized, so I do not stop production)
sulfur vulcanization accelerators
  discovered at the beginning of the 20th century
  today mainly mercaptobenzothiazole derivatives
  dosage according to the intended result
    accelerator:sulfur ratios tend to be:
      1:5 to 1:2 for so-called conventional vulcanization
      1:1 for semi-effective vulcanization
      5:1 and more for effective vulcanization
    the total amount of sulfur is not more than 2.5 phr
bis(2-benzothiazolyl)disulfide
sulfenamide accelerator

## Slide 29: Networking accelerators
sulfur vulcanization accelerators
  sulfur donor accelerators
    they can also be used alone (without the addition of sulfur = so-called sulfur-free vulcanization), so they are both an accelerator and a crosslinker at the same time
  ultraaccelerators
    reduce vulcanization temperatures (warm water or even room temperature is enough)
    generally zinc or sodium salts of more complex organic substances
      used mainly for cross-linking latexes
        these contain so much water that if they cross-linked at 100 °C, the product would be damaged by evaporation
        laboratory gloves, balloons, etc.
  dosage up to 1.5 phr
types of vulcanization accelerators according to speed
slow
fast
very fast
ultrafast

## Slide 30: Curing accelerators
different substances depending on the cured reactoplast
  metal salts of organic acids for curing silicone resins
    Co, Pb, Zn
  amines for curing polyester resins or epoxy resins

## Slide 31: Other additives

## Slide 32: Other additives
affects all sorts of properties
types:
  fillers
  reinforcements
  puffed up
  pigments
  optical brighteners
  plasticizers
    they belong to processing additives, but since they also affect the final properties, they can also be included here

## Slide 33: Fillers
solids in the form of powder or fibers (length in units of mm)
they influence
  price
  density
  strength
  abrasion resistance
  toughness
  resistance to higher temperatures, aging
  appearance
all sorts of dosages

## Slide 34: Fillers - carbon black
most often in the rubber industry
Ingredients
  H … 0.3 – 0.6%
  About ... 0.1 - 3.5%
  C … 96 – 99%
  the composition is determined by the type of carbon black, which is classified according to several aspects (production method, surface area, etc.)
they are obtained as industrial waste (burning residues)
rubbers improve
  strength
  rigidity
  abrasion resistance
  possibly electrical conductivity + antistatic effects
impair workability (the polymer mixture is more viscous)
dosage according to the product up to about 50 phr

## Slide 35: Light fillers
all other rubber fillers other than carbon black
usually inorganic substances
  SiO2
  CaSiO3
  hydrated aluminum sulfite (kaolin)
  CaCO3 (chalk or limestone)
  barite (BaSO4) – together with PbSO4 act as shielding substances for high-energy radiation
  MgSiO3 (talc)
  glass fibers
also organic
  cellulose (wood meal, fruit shell meal)
  protein flours (soy, casein)

## Slide 36: Stiffeners
most often with reactive plastics and thermoplastics
especially fibers
  cellulose fibers
  PE
  PA
  glass
  metal (in combination with rubber, the so-called rubber bands)
they improve the mechanical properties of the product
they often lighten the overall structure

## Slide 37: Puffing agents
they make the product lighter and cheaper
substances added to the polymer mixture that decompose due to the formation of gases at a higher temperature (e.g. during molding).
  most commonly CO2 or N2
  they form open and closed pores in the material
  they basically act like baking powder or yeast (but they create CO2 in a different way) in the dough
formerly inorganic salts (ammonium or sodium)
today organic blowing agents
  usually nitrogenous substances
  pentane works for PS (when cooking PS with pentane inside, it starts to evaporate and puffs up the final product)
dosage from 1 to 5 phr

## Slide 38: Pigments
colored particles (powders) insoluble in the carrier (polymer)
  inorganic
  organic
  metal (bronze)
inorganic
  chalk, gypsum, graphite
  zinc white (ZnO), titanium white (TiO2), ZnSO4, BaSO4, lemon yellow (FexAlySizOm), red (Fe2O3), synthetic ultramarine (silicate complex), carbon black
  cheap, good stability, poor coverage and discolouration

## Slide 39: Pigments
organic
  together with white base (TiO2)
  dosage 0.5 to 2 phr color pigment, up to 10 phr whiteness
  chelates of organic substances with metals
    yellow – Cd (not so much these days), Ni
    blue - copper
    red – iron
    green - copper, iron
anthraquinone
azobenzene
isoindolidone

## Slide 40: Optical brighteners
they absorb wave radiation at the limit of visible light and emit UV and fluorescence back at higher wavelengths
  simplified – incident radiation slightly below 400 nm is used to emit visible radiation around 450 nm
  the whole appears brighter and more colorful
  they are used a lot in the paper industry
  may not be compatible with other radiation-absorbing substances (light stabilizers, ZnO, TiO2)
usually a system with at least 4 conjugated double bonds - stilbene derivatives
dosage 0.01 to 0.001 phr
stilbene

## Slide 41: Special additives

## Slide 42: Special additives
they are only added to polymers with special uses
types:
  antistatic
  adhesives
  reducing flammability
  abrasives
  explosives and fuels

## Slide 43: Antistatic agents
Antistatic agents helping to remove the charge from the surface of the polymer product
the charge accumulates on the surface, e.g. when rubbing or unwinding foils, because most polymers are poor current conductors
  problems with attachment to the device and everything possible in the vicinity
  in extreme cases, there may be a spark jump that can cause a fire
antistatic agents increase conductivity, thus the accumulated charge is able to be removed
  carbon black or a lot of polar organic matter works well
dosage from 0.1 to 2 phr
  it usually does not need to be added to rubbers, because there is conductive carbon black (as a filler)

## Slide 44: Adhesives
they improve the adhesion between the polymer and other substances (especially reinforcement)
  important for textiles, laminates, tires, conveyor belts, etc.
depending on the type of polymer-adhesive, different substances are used
  usually organometallic complexes or resins
dosage in units of phr

## Slide 45: Flame retardants – Hoření polymerů
generally flammable with a low degree of fire safety
  in other words, it burns well, quickly and easily
the limiting factor in the use of polymers
combustion research
  mechanism
  reducing flammability
fire triangle
  the relationship of the main factors of combustion
  removing only one means preventing burning
fuel
oxidizer (oxygen)
energy source (heat)

## Slide 46: General course of combustion
initiation heat with oxygen will start the thermo-oxidation reaction of the polymer
the result is oxidation of the polymer
  release of heat of reaction (further heats the system)
  formation of by-products
an increase in temperature results in thermal decomposition of the oxidized polymer
  the formation of volatile flammable substances that further oxidize and add additional heat
  formation of solid products that may or may not further support combustion

## Slide 47: Classification of materials according to flammability
Non-flammable products
  A1 ... products made of ceramics, glass, metal, concrete, thermal insulation board made of mineral fibers
  A2 … plasterboard or plasterboard
Flammable products
  B … contact insulation system with combustible thermal insulation (e.g. expanded polystyrene), vinyl floors, cement chipboards
  C ... thermal insulation board made of phenolic foam
  D ... construction wood, wood-based boards
  E ... thermal insulation board made of polyurethane or expanded polystyrene (with flame retardants)
  F ... products for which the class has not been determined
significant material values:
  flash point (FP = the lowest temperature at which a substance ignites and goes out again when approached by a flame
  flame ignition temperature (FIT) = the lowest temperature at which a substance spontaneously ignites
PE, PP and PMMA are very flammable
there are few non-flammable polymers
  PTFE or FEP (copolymer of tetrafluoroethylene and hexafluoropropylene), polyimides, silicones
those containing halides (PVC) or highly cross-linked tend to be self-extinguishing

## Slide 48: Influence of flammability
flammability is affected by:
  structure of monomers
  branching (reduces)
  by cross-linking (reduces)
  additives
    some may promote combustion (e.g. volatile organic solvents)
    some may reduce or at least not support (e.g. inorganic fillers, flame retardants)
  the size of the polymer surface
    the fibers will burn much more easily than the whole body
  barrier from decomposition products
    charred residues can form a layer that is poorly permeable to oxygen and prevent further combustion

## Slide 49: Limiting oxygen index
LOIestimation of the material's flammability relative to the oxygen content in the air
  defined as the representation of oxygen in the atmosphere consisting of only oxygen and nitrogen, necessary to burn through exactly 50% of the sample
  the higher the number a given material has, the more durable it is
it is tested by igniting a sample in a tube through which a mixture of oxygen and nitrogen of known composition is blown

## Slide 50
polymer | abbreviation | CU formula | elemental composition (wt. %) |  |  |  |  | LOI 20 °C (%)
 |  |  | H | C | N | O | halogen | 
polyethylene | PE | [C2H4] | 85,7 | 14,3 | - | - | - | 17,5 – 18,5
polypropylene | PP | [C3H6] | 85,7 | 14,3 | - | - | - | 18,0 – 19,0
polymethyl-metacrykate | PMMA | [C5H8O2] | 60,6 | 8,0 | - | 32,0 | - | 17,3
polyvinylchloride | PVC | [C2H3Cl] | 38,4 | 4,8 | - | - | 56,8 | 30,0 – 45,0
butadien rubber | BR | [C4H6] | 88,9 | 11,1 | - | - | - | 17,5 – 18,5
phenoplasts | PF | [C7H7] | 78,5 | 6,5 |  | 15,0 | - | 28,0 – 35,0
polyurethane | PUR | [C12H22N2O4] | 55,8 | 8,5 | 11,2 | 24,8 | - | 19,0 – 20,0
polystyrene | PS | [C8H8] | 92,3 | 7,7 | - | - | - | 18,0 – 20,0
polytetrafluor-ethene | PTFE | [C2F4] | 24,0 | - | - | - | 76,0 | 95,0 – 98,0
CU … constitutional unite

## Slide 51: Flame retardants
substances (or parts of macromolecules) with the task of slowing down or completely preventing the burning of the material
principles of flame retardancy
  endothermic reaction
    the excess heat is used for a reaction that does not support combustion
  formation of non-flammable gases
    they dilute the air and thus reduce the relative amount of oxygen
  dehydration
    excess heat is used to split and evaporate water, which further dilutes the air and reduces the relative amount of oxygen
  melting
    excess heat is used to melt the material, which can also form an oxygen-impermeable barrier
  deactivation of free radicals
    the resulting free radicals are deactivated by other substances and thus help to slow down the thermal-chemical decomposition of the substance (e.g. they deactivate HCl or HBr)

## Slide 52: Flame retardants
inorganic compounds
  Al2O3xH2O, Zn(BO2)2, NH4Cl, (NH4)3PO4, Sb2O3
organic compounds with halides
  chlorinated (CFR = Chlorinated Fire Retardants) or brominated (BFR)
    they work on the principle of capturing HO· or H· radicals produced by combustion, which further support combustion with the help of hydrogen halide HX – which itself is produced by the thermal decomposition of the retarder
    I can either add it as an additive to the polymer or as a comonomer in the production of the copolymer
  bromine is more commonly used (and more effective)
  chloroparaffin, hexachlorobenzene, tetrabromobisphenol A, tetrabromophthalic anhydride etc.
organic compounds with phosphorus
  a combination of flame retardant and plasticizer
  triscresyl phosphate
  organic halogenated phosphorus compounds

## Slide 53: LOI after adding a retardant
polymer | LOI | LOI after the addition
PES | 21 % | 28 %
viscose | 17 – 19 % | 30 %
cotton | 18 – 20 % | 31 – 32 %
wool | 24 – 25 % | 33 %

## Slide 54: Abrasives
hard abrasive particles in a polymer matrix
the polymer here serves only as a binder
  most often hard rubber (in addition to abrasives, there is also a meshing agent, etc.)

## Slide 55: Explosives and fuels
polymer mixture with explosive = plastic explosive
usually rubbers or thermoplastic rubbers
the fuel can be e.g. gasoline
  solid fuels can also be produced in this way

## Slide 56: Thank you for your attention