## Slide 1
Inovace stávajících nebo tvorba nových metodických a elektronických studijních materiálů v ČJ nebo AJ
Ing. Pavel Holec
Nové možnosti rozvoje vzdělávání na Technické univerzitě v Liberci
Specifický cíl A2: Rozvoj v oblasti distanční výuky, online výuky a blended learning
NPO_TUL_MSMT-16598/2022

## Slide 2: Special polymers

## Slide 3: Production of special polymers
large tonnage
  most of the volume/mass of the polymers produced
  PE, PP, PS, PVC, PES, PA
special
  electrotechnics
  cosmonautics
  medicine
  the military
today the focus of polymer research
significant price difference between regular and specialty polymer

## Slide 4: Production of special polymers
LCP,
PEEK, PPS
PET, PA
PBT, PC, ABS,
POM, PMMA
HDPE, LDPE,
LLDPE, PP, PVC, PS
price
mass produced
Notes: PPS = polyfenylensulfid

## Slide 5: Special polymers
resistant to higher temperatures
super absorbent
liquid crystals
electrically conductive
photosensitive polymers
ion exchangers
self-healing
polymers in medicine
Notes: Airloy – aerogel (polymerní, keramický, kovový aj.) (0,01 g až 0,9 g na ml) – nízká hustota + vysoká izolační odolnost
třeba polyimid, polyuretan, polyamid

## Slide 6
Polymers resistant to higher temperatures

## Slide 7: Examples of heat-resistant polymers
usually in fiberglass composite
polyphthalamide (PPA)
  Tg up to 127 °C, Tm up to 310 °C
  a relatively inexpensive temperature-resistant variation on PA6 or PA66
aromatic polyamides (aramids)
  Nomex – Tm around 350 °C, use up to 220 °C
  Kevlar – Tm around 330 °C, use up to 200 °C
polyetherimide (PEI)
  long-term stable up to 170 °C
polyimides (PI)
  long-term stable up to 260 °C

## Slide 8: Polyphthalamide and polyaramids
terephthalic acid
pentane-1,5-diamine
building block of polyphthalamide (NILON 6T)
Nylon 5T
Kevlar
Nomex

## Slide 9: Polyetherimide and polyimide
PEI
imides in general
4,4'-diaminodiphenyletheroxydaniline
diphenylether-4,4'-diisocyanate
pyromellitic acid dianhydride
PEI
amide of two carboxylic acids
Notes: A = obvykle bisfenol (obecně dihydroxydifenylmethan), ale lze i spousta dalších

## Slide 10: Preparation of polyimides
aromatic diamine
pyromellitic acid
1. step
200 °C
2. step
250 °C
PI

## Slide 11: Examples of heat-resistant polymers
polysulfones (PSUs)
  Tg up to 250 °C
  good mechanical properties, chemically resistant
polyphenylene sulfide (PPS)
  Tm around 290 °C
  easy processing of the melt (good flow properties)
polyether ether ketone (PEEK)
  Tg up to 145 °C, Tm up to 335 °C
  good mechanical properties, dimensional stability at higher temperatures, bioinert
polybenzimidazole (PBI)
  Tg around 430 °C, short-term withstand over 700 °C
  the highest temperature resistance of commercially produced polymers
  mechanically very resistant

## Slide 12: Polysulfones and polyphenylene sulfide
sodium polysulfide (X is not higher than 5)
PSU
PPS

## Slide 13: Polyetherketone
PEK
PEEK
PEKK
PEEKK
Tg [°C] | Tm [°C]
163 | 361
144 | 344
154 | 358
165 | 391

## Slide 14: Polybenzimidazole
3,3',4,4'-tetraamin biphenyl
PBI
isophthalic acid
ΔT
ΔT

## Slide 15: Novoloid (Kynol)
from melt-spun phenol-formaldehyde "resin" subsequently cross-linked to the maximum extent possible
  probably from slightly cross-linked novolacs = phenoplasts resulting from the reaction of phenol with formaldehyde, where there is an excess of phenol
the result is a three-dimensional amorphous network
further infusible, heat-resistant, but basically flammable
  relatively chemically resistant, but does not benefit from conc. H2SO4 or conc. HNO3
  LOI 30 – 34 (PVC has 30 – 45, PTFE up to 98)
classified as novoloids, which are at least 85% cross-linked novolacs
  Kynol is the only representative so far 😂
very well described from commercial perspective:
  withstands up to 2500 °C for at least 12 s
  can withstand 200 – 250 °C for a long time in an oxygen-free atmosphere
  long-lasting up to 150 °C in air

## Slide 16
Super absorbent polymers

## Slide 17: Super absorbent polymers (SAP)
polymers capable of binding more than 300 times their weight (in a dry state) of distilled water
they replace older cellulose sorbents (pulp, cotton)
two ways of sorption
  to polar groups (-OH, -O-, -CO-NH2)
    older SAPs from derivatives of cellulose, starch, gelatin (gummy bears), PVA, PEO or PAM (polyacrylamide)
    they sorb less, but are not as sensitive to liquid composition
  per ionic charge
    today mainly slightly cross-linked polyacrylic acid
    they absorb a lot, but are sensitive to the composition of the liquid
PAM

## Slide 18: Sorptive capacity
dry SAP (sorbing by ion mechanism)
  distilled water ... up to 300 times the weight
  physiological solution (0.9% NaCl) ... up to 50 times
ions in water reduce the sorption capacity
pressure on the SAP reduces the sorption capacity
  like wringing a wet rag
swelling creates a hydrogel (substance made up mainly of water, which, however, retains certain mechanical properties, shape, etc.)

## Slide 19: Polyacrylic acid (PAA)
it is not a homopolymer, but a copolymer of acrylic acid and a cross-linking monomer (N,N'-methylene-bis-acrylamide)
a high molecular weight polymer is to be obtained
  otherwise, the insufficiently cross-linked part could wash out
  the mass of PAA that can be extracted in this way is usually 5 to 20% by weight
production process:
  copolymerization of acrylic acid with a cross-linking comonomer
  neutralization by NaOH
  replacing part of the -COOH groups with its sodium salts –COONa
  at the same time, the pH value of the prepared SAP is thus adjusted
  drying and grinding
  surface finishes
  additional surface cross-linking of the ground particles so that, during water sorption, the surface of the particles does not swell quickly and the formation of a gel-like cluster, which is also poorly permeable to water

## Slide 20: A simplified scheme of the polymerization of acrylic acid
cross-linking comonomer N,N'-methylene-bis-acrylamide

## Slide 21: Cross-linked and partially neutralized PAA
cross-linking comonomer N,N'-methylene-bis-acrylamide

## Slide 22: PAA cross-linking
provides:
  insolubility of the resulting product
  mechanical properties of the resulting hydrogel
  reduces the amount of extractable components (linking macromolecules increases the average molecular weight)
the more cross-linked the PAA, the stronger the hydrogel, but the less it can sorb
  PAA then cannot swell as much
cross-linking comonomers
  N,N'-methylene-bis-acrylamide
  trimethylolpropane triacrylate (TMPTA)
crosslinking of PAA homopolymer
  ethylene glycol diglycidyl ether (EGDGE)
    reacts with ready-made PAA macromolecules

## Slide 23: Water sorption and PAA swelling
water with secondary bonds binds to charged or partially charged parts of macromolecules and to ions trapped inside the network
the difference of osmotic pressures inside the PAA and in the sorbed liquid
  cations inside the PAA network (e.g. Na+) are practically not washed out, because they are held by a large number of partially negatively charged parts of the macromolecules
segments of chains of the same charge that come too close repel each other
  thus helping the hydrogel to expand

## Slide 24
Polymer liquid crystals

## Slide 25: Liquid crystals
1888 – discovery of liquid crystals (F. Reintzer)
the liquid-crystalline phase in polymeric substances was described by Paul John Flory (1954 onwards)
the first liquid-crystalline polyester on the market in 1972
  Ekkcel I-200
significantly anisotropic molecules that can change their orientation in space under the influence of a force field
transition between isotropic and anisotropic matter

## Slide 26: Liquid crystals
formed by mesogens
  a molecule or part thereof, responsible for liquid-crystalline behavior
  rod-shaped or disc-shaped (one or two dimensions significantly different)
creates oriented structures in the external force field
  after orientation, they show different optical, electrical and magnetic properties, density, etc.
types:
  lyotropic liquid crystals
    molecules with mesogens dissolved in a foreign liquid phase
  thermotropic liquid crystals
    molecules with mesogens acting in the mass above the melting temperature
  smectic phase (highly symmetric even at long distances)
  nematic phase (less symmetric and rather at shorter distances)
    solid ↔ smectic ↔ 𝑛𝑒𝑚𝑎𝑡𝑖𝑐 ↔ liquid
an increase in T

## Slide 27: Polymer liquid crystals (LCP)
mesogens as a repeating part of a macromolecule
thermotropic
  only works above Tg
a combination of rigid (rods or disks) and flexible segments
  on the main chain
    chain-like
  off the main chain
    orthogonal
    ridge-like

## Slide 28: Polymer liquid crystals (LCP)
orthogonal LCP
(mesogens off the main chain)
chain-like LCP
(main chain mesogens)

## Slide 29: Polymer liquid crystals (LCP)

## Slide 30: Examples of mesogens
only works above Tg
R … flexible group
X and Y ... inflexible groups
  alkene, alkyne, ester, amide, secondary (ald)imine, azo compound
alkylene
alkoxy
alkendiyl
(vinylen)
alkyndiyl
ester
secondary aldimin
azo compound
Notes: (ald)imin

## Slide 31
Electroconductive polymers

## Slide 32: Electroconductive polymers
polymers are usually insulators
increasing the conductivity of the polymer
  polymer with conjugated e- in the main chain
    conjugated chain → movable π e-
    representatives
      polyacetylene (ie polyethylene)
        conductivity comparable to metals
        it burns in the air
      polyaniline
      polyphenylene-vinylene
        pure aromatic backbone
      poly(p-phenylene)
      polythiophene
      polypyrrole
  redox doping (supplied e-)

## Slide 33: Electroconductive polymers

## Slide 34: Electroconductive polymers

## Slide 35: Use of electroconductive polymers
anti-corrosion protection of metals
accumulators
  many times lighter than the existing one
electrochromic devices
  the electrically conductive polymer can have a different color in its original and doped state
  information storage
gas separation
  oxygen-nitrogen, methane-CO2
  with repeated doping of polyaniline, pores of a defined size will be formed

## Slide 36: Redox color changes of polyaniline

## Slide 37
Photosensitive polymers

## Slide 38: Photosensitive polymers
not to be confused with photopolymers
  synthetic resins cured by (usually UV) radiation
changes the structure under the action of light
  returnable
  irreversibly
classic photography – photosensitive substances applied in emulsion (defined particle size)
  they allow for virtually infinite magnification
    to the size of the molecules – “What more would you like to see? Quarks?”
  change in structure → change in optical density
    optical data storage
  medicine

## Slide 39: Photosensitive polymers
photocyclization of triisopropyl-benzophenones

## Slide 40
Polymer ion exchangers

## Slide 41: Polymer ion exchangers (ionex)
acidic or basic functional groups on a suitable polymer support
water softening
  originally for steam boilers
  water demineralization
  extraction of precious metals from very dilute solutions
accumulators

## Slide 42: Ion exchangers (cathexes)
cathexes
  e.g. PS porous copolymer with divinylbenzene (crosslinker) + functional group (sulphonic -SO3H)

## Slide 43: Ion exchangers (annexes)
annexes
  e.g. PS porous copolymer with divinylbenzene (crosslinker) + functional group (quaternary ammonium salt)

## Slide 44
Self-healing polymers

## Slide 45: Self-healing polymers
they convert the mechanical energy into that which allows the broken chain to be linked with other chains
  physically
    diffusion of macromolecules to a new surface
    entanglement of macromolecules into a physical network
  physico-chemical
    diffusion of macromolecules to a new surface
    the formation of a covalent or supramolecular network
      reversible or irreversible

## Slide 46: Surface bonding methods
diffusion of molecules
chemical reaction
mechanical damage

## Slide 47: Physical bonding of surfaces

## Slide 48: Physico-chemical bonding (irreversible)

## Slide 49: Examples of reversible cross-linking

## Slide 50
Ostatní

## Slide 51: Baropolymers
polymers that respond to pressure by melting at normal temperatures
  non-crosslinked block polymers
the possibility of recycling without the need for heating
  does not reduce the average degree of polymerization by thermal degradation
  can be repeated many times (not just 2-3 times)
given by the change in phase equilibrium
  phase of block A and phase of block B can be separated at a given pressure and temperature (I have 2 phases)
  by reducing the pressure, the curve can be lowered and the point will reversibly reach the region of unlimited miscibility
  after re-reducing the pressure back solidification
limited miscibility
H
unlimited miscibility
TH
higher pressure

## Slide 52
Polymers in medicine

## Slide 53: Biocompatible polymers
must meet the characteristics given by law
must not cause side reactions in the body (e.g. allergies)
  they should be inert in the body environment
  few residues (according to the tables)
UHMWPE, PP, PA6 (threads), PEEK, PTFE, PVDF

## Slide 54: Biodegradable polymers
must meet the characteristics given by law
they degrade in the body environment without side effects
  degradation is known in advance, "controlled"
degradation time of the polymer in the body
  applicability
  the time during which the material retains its mechanical property
  complete resorption
  the time it takes for the body to break down the material so much that it is not noticeable
diferentiation by origin
  natural
    chitosan, collagen, hyaluronic acid (mainly bacterially formed, formerly from animal bodies), alginates
    now on the decline (badly modified, difficult repeatability of production)
  synthetic
    polycaprolactone, polylactic acid, polyglycolic acid, polylactic/polyglycolic acid copolymers (various proportions), polydioxanone, bacterial biodegradable polymers (hydroxybutyrates, hydroxyvalerates, hydroxysuccinates), polyurethanes

## Slide 55: Example:
contact lenses
  poly(hydroxyethyl) methacrylate (HEMA)
  gel structure (relatively tolerable for the eye)
    Otto Wichterle
    MERCURY
    disadvantageously patented
protective packaging of medicines
polymeric drug carriers
prosthetics

## Slide 56: Thank you for your attention

## Slide 57: Merry Christmas